UNIT II

Mechanical Finish

Mechanical finishes – methods and applications; Aesthetic finishes: Luster – glazed, moiré, schreiner, embossed; Drape – crisp and transparent, burnt out,sizing,weighting;Texturesheared,brushed,embossed,plisse,pleated,flocked,embroidered,napped,fulled;

MECHNICAL FINISHES

METHODS AND APPLICATION:

CALENDERING

Calendering may be defined as the modification of the surface of a fabric by the action of heat and pressure. The finish is obtained by passing the fabric between heated rotating rollers (or bowls as they are frequently called), when both speed of rotation and pressure applied are variable. The surfaces of the rollers can be either smooth or engraved to provide the appropriate finish to the fabric, while the actual construction of the rollers may be varied from hardened chromium-plated steel to elastic thermoplastic rollers.

Effects which may be achieved by calendaring

Calendering is done for many purposes but the main effects are:

• smoothing the surface of the fabric

• increasing the fabric lustre

• closing the threads of a woven fabric

• decreasing the air permeability

• increasing the fabric opacity

• improving the handle of a fabric, i.e. softening

• flattening slubs

• obtaining silk-like to high gloss finishes

• Surface patterning by embossing

• Consolidation of nonowners.

Types of calendar

In general Calenders usually have between two and seven rollers, with the most common being the three-bowl Calender. Perhaps the most important factor in Calender design is the composition of the rollers and the surface characteristics of these. Textile Calenders are made up from alternate hard steel and elastic bowls.

The elastic bowls are made from either compressed paper or compressed cotton, however, a lot of modern Calenders are made with a thermoplastic thick covering, which is usually nylon6. The latter have the advantage that they are less liable to damage from knots, seams and creases than cotton and paper bowls, damage that would then mark off onto the calendered fabric.

In two-bowl Calenders it is normal to have the steel bowl on top so that the operator can see any finish. This type of arrangement is often used with the nylon bottom bowl mentioned previously, especially where the Calender is used for glazing or the embossed type of finishes.

The arrangement where two steel bowls are used together only occurs in exceptional

Circumstances, for example, in the compaction of nonowners. Here both bowls are usually oil heated so that some form of permanent setting occurs. Finally, the arrangement with two elastic bowls is not common but is sometimes used on cotton knit goods to obtain a soft handle.

The three-bowl Calender was developed from the two-bowl calendar and with this type of Calender it is normal to use only the top nip, with the bowls arranged steel–elastic–steel. The bottom bowl is used to keep the central elastic bowl smooth and thus assist in the finishing. The same arrangement also serves the same purpose on embossing Calenders, where there is the possibility of permanent indentation from the top roller.

Pressure used in all of the above Calenders can be varied between 10 and 40 tonnes, with running speeds up to 60mmin-1. However, these are very much average figures with figures as low as 6 tonnes for a 1m wide Calender to as high as 120 tonnes for a 3m wide Calender. In addition, running speeds of 20mmin-1 are used on an embossing Calender, while on a glazing Calender speeds of over 150mmin-1

The temperatures which are used in Calender rollers can, of course, vary from room temperature to 250°C.However, it must be stressed that temperature control is of vital importance, with a tolerance of ±2 °C being commonly quoted.

Cold bowls give a soft handle without much lustre; warm bowls (40–80 °C) give

a slight lustre.

• Hot bowls (150–250 °C) give greatly improved lustre, which can be further improved by the action of friction and waxes.

Types of finish

• Swissing or normal gloss: a cold Calender produces a smooth flat fabric. However, if the steel bowl of the Calender is heated then in addition to smoothness the Calender produces a lustrous surface. If a seven-bowl multipurpose calendar is used then a smooth fabric with surface gloss on both sides is produced.

• Chintz or glazing: this gives the highly polished surface which is associated with glazed chintz. The effect is obtained by heating the top bowl on a three-bowl Calender and rotating this at a greater speed than that of the fabric. The speed of this top bowl can vary between 0 and 300% of the speed of the fabric. In certain cases where a very high gloss is required, the fabric is often pre impregnated with a wax emulsion, which further enhances the polished effect. This type of calendering is often called friction calendering.

• Embossing: in this process the heated top bowl of a two-bowl Calender is engraved with an appropriate pattern which is then transferred to the fabric passing through the bowls. The effect can be made permanent by the use of thermoplastic fibres or in the case of cellulosics by the use of an appropriate cross linking resin.

• Schreiner or silk finishing: this is a silk-like finish on one side of the fabric. It is produced by embossing the surface of the fabric with a series of fine lines on the surface of the bowls. These lines are usually at an angle of about 30° to the warp threads. The effect can be made permanent by the use of thermoplastic fabric or, in the case of cotton, by the use of a resin finish. This finish is particularly popular on curtains and drapes because of the silk-like

appearance this type of finish gives to the product.

• Delustering: this is commonly achieved by passing the fabric through the bottom two bowls of a three-bowl Calender, where these are elastic. However, steel bowls with a special matt finish have been manufactured that are very effective for this purpose.

• Chasing: the fabric is threaded through the Calender in such a way as to press the fabric against itself several times. It is common to use a five- or seven-bowl Calender, the fabric passing through each nip of the Calender in two or three layers.

Palmer finishing: in this type of finish the damp fabric is carried on the inside of a felt blanket round a steam-heated cylinder, often called a Palmer drier. The face of the fabric, which is run on the surface of the heated cylinder, takes a light polish from the cylinder, while the back of the fabric, which is in contact with the felt blanket, takes a roughened effect from the cylinder. This finish is particularly popular for cotton drill fabric. These descriptions of calendering should not be regarded in any way as complete and for a more complete description the reader is recommended to contact the calendar manufacturers. Some of these are Küsters in Germany, Parex Mather in the UK, Kleinewefers in Germany and Metallmeccanica in Italy.

RAISING

Raising is the technique whereby a surface effect is produced on the fabric that gives the fabric a brushed or napped appearance. It is achieved by teasing out the individual fibres from the yarns so that they stand proud of the surface.3 The way this was done originally was to use the seedpod of the thistle, which was known as a teasel. These teasels were nailed to a wooden board and the fabric was drawn over them to produce a fabric with a hairy surface, which had improved insulating properties.

This method has largely been superseded by the use of rotating wire brushes,

Although where a very gentle raising action is required, such as in the case of mohair

Shawls, teasels are still used.

Modern raising machines

All modern raising machines use a hooked or bent steel wire to tease the fibres from the surface of fabric. The most important factor in the raising operation is the relationship between the point and the relative speed of the cloth. The raising wires or ‘card’ wires are mounted on a flexible base, which is then wrapped around a series of rollers, which are themselves mounted on a large cylindrical frame,

The raising action is brought about by the fabric passing over the rotating rollers and the wire points teasing out the individual fibres in the yarn. Because there area large number of points acting on the fabric at any one time, the individual fibres must be sufficiently free to be raised from the fibre surface. This is a combination of the intrafibre friction and the degree of twist in the raised yarns. Thus for ‘ideal’ raising, the yarns should be of low twist and be lubricated. One further point to note is that because the fabric runs in the warp direction over the machine, only the weft threads are at right angles to the rotating raising wires and therefore only the weft threads take part in the raising process.

Raising action

That both the card wire rollers and the cylinder to which these are attached may be rotated; it is the relative speed of these in relation to that of the fabric that produces the various raising effects that may be achieved.

There are two basic actions in raising and these are governed by the direction in which the card wires point and the relative speed of rotation of these in relation to the fabric. These actions are called the pile and the counterpile actions

In the counterpile action, the working roller rotates in the opposite direction to that of the cylinder with the points of the wire moving in the direction of rotation. This action pulls the individual fibres free from the surface.

In the pile action, the points of the wire are pointing away from the direction of movement of the fabric. This results in an action where the raised fibres are subject to a combing action which tends to tuck back the fibres into the body of the fabric. The most common raising action uses a combination of both of these actions, producing an even raise over the whole of the fabric surface. Control of the raising action has been achieved by measurement of the surface roughness of the raised fabric. It is therefore possible to control the exact height of the nap on the surface of fabrics.

SHEARING

This is a process by which the fibres which protrude from the surface of a fabric, are cut to an even height. The principle used in this technique is similar to a lawn mower in that a spiral cutter rotates against a stationary blade and cuts off any material protruding from the fabric surface.

This principle, in  which shows the fabric passing over the cutting bed and the protruding hairs on the surface being caught between the rotating head of the spiral cutter and the ledger blade. By raising and lowering the height of the cutting bed, the depth of cut may be varied. Obviously the cutting action produces a great deal of cut pile and this must be removed by strong suction otherwise a large amount of fly rapidly accumulates. In order to achieve an even cut and a smooth surface, several passes through the machine are required or a single

pass through a multiple head machine is required. Average speeds of about 15mmin-1 are commonly encountered.

One important use for this technique is the production of pile fabrics from a looped terry fabric. When this type of fabric is sheared the top of the loops of the terry fabric are cut off and a velvet like appearance is produced. When knitted loop pile fabrics are sheared, knitted velour is produced that has found a great deal of use in upholstery fabric.

COMPRESSIVE SHRINKAGE

The shrinkage of fabrics on washing is a well-known phenomenon. It is caused in part by the production and processing stresses on the fabric. Production stresses are introduced into the fabric by the yarn tension and also by the tension which is necessary for the satisfactory production of fabric. Processing stresses are introduced during the bleaching, dyeing and finishing of fabric when the fabric is pulled in the warp direction. This tends to remove the warp crimp from the fabric

In order to replace the warp crimp and thus minimise warp shrinkage, a process known as compressive shrinkage is carried out on the fabric to replace the crimp that has been pulled out in the preparation and finishing processes. A strip of fabric is placed on a convex rubber surface and gripped at each end of the rubber. As the rubber is allowed to straighten, the

length of the fabric exceeds that of the rubber . However, if the fabric could be stuck to the surface of the rubber then the fabric would be subjected to compression and warp crimp would be introduced.

AESTHETIC FINISHES

Aesthetic finishes change the appearance and / or hand of fabrics. The finished fabric’s name often reflects the change in appearance or the technique.

LUSTER FINISH

Luster finishes produce a change in a fabric’s light reflectance. Most of these finishes increase light reflectance and improve the fabric’s luster or shine. The increase in luster may be over the entire fabric as in the glazed, cire, and schreiner finishes or it may be localized increase in luster as in the moiré and embossed finishes. These finishes are done by calendaring passing the fabric between two cyclinders. The cyclinders exert pressure on the fabric. Different calenders produce different effects on the fabric: glazed, cire, moiré, schreiner and embossed.

GLAZED

Glazed chintz and polished cotton are two fabrics that received surface glazing. A friction calendar produces a highly glazed surface. If the fabric is first saturated with starch and waxes, the finish is temporary. If resin finishes are used, the glaze is durable. The fabric is passes through the finishing solution and partially dried. It is then calendared. The speed of the metal roller is greater than the speed of the fabric, and the roller polishes the surface.

Moire

Moire fabrics have a wood grain or watermarked appearance. Two techniques are used to produce a moiré pattern on a fabric. In true moiré, two layers of an unbalanced plain-weave rib fabric such as taffeta or faille are placed face to face so that the ribs of the top layer are slightly off-grain in relation to the under layer. The two layers are switched or held together along the selvage and or then fed into the smooth heated-metal-roll calendar. Pressers of 8 to 10 tons cause the rib pattern of the top layer to be pressed into the bottom layer and vise - versa. Flattened areas in the ribs reflect more light and contract with un flattened areas. This procedure can be modified to produce patterned moiré designs other than the traditional watermarked one.

In the second technique, an embossed-metal roll is used. The embossed roll has a more pattern engraved on it. When the roll passes over a ribbed fabric, the ribs are flattened in areas and amore pattern is created. If the fabric is thermoplastic and the roll is heated, the finish is permanent . Different pattern can be achieved depending on the pattern on the embossed roll. The repeat of the pattern of the related to the diameter of the embossed roll.

Schreiner

Fabrics with a schreiner finish have a softer luster than most of the other luster finish. The schreiner calendar has a metal roller. engraved with 200 to 300 fine diagonal lines per inch that are visible only under a magnifying glass. (The line should not be confused with yarn twist.) Unless resins and thermoplastic fibers are used, this finish is temporary and removed by the first washing. This finish scatters light rays and produces a deep-seated luster rather than a shine. It also flattens the yarns to reduce the space between them and increase smoothness and cover. It can upgrade a lower-quality fabric. A schreiner finish is used on cotton sateen and table damask to make them more lustrous and on nylon tricot to increase its cover.

Embossed

Embossed fabrics are created using an embossing calendar that produces either flat or raised designs on the fabric. Embossing because a more important finish with the development of the heat-sensitive fibers because it became possible to produce a durable, washable embossed pattern. Fabrics made of solution-dyed fibers can be embossed directly off the loom and sold.

The embossing calendar consists of a heated, hollow engraved-metal roll and a solid paper roll twice the size of the engraved roll. The fabric is draw between the two rollers and is embossed with the design. Embossing can be done to both flat and pile fabrics.

The process differs for the production of flat and raised designs. Raised embossed designs will be discussed later in this chapter in the section on texture. Flat embossed designs are the simplest of produce. A metal, foam, or plastic roll engraved in deep relief revolves against a smooth paper roll. The hot engraved against a smooth paper roll. The hot engraved areas of the roll produce a glazed pattern on the fabric. Embossed brocades are an example of this type of design. The effect can be seen as a different in luster, but the fabric’s texture does not change.

DRAPE FINISH

CRISP AND TRANSPARENT

Transparent effects in cotton fabrics are produced by treatment with sulphuric acid: this is called parchmentizing. Since acid dissolve cotton, this subtractive process must be very carefully controlled. Split-second timing is necessary to prevent tendering of the fabric. Several effects are possible: an all over, a localized, or a plisse effect.

Because all over parchmentizing produces a transparent effect, sheer combed lawn is used. The lawn is singed, desized, bleached, and mercerized. The fabric is then dyed or printed with colours that resist acid damage. The fabric is immersed in the acid solution and the fiber surface is partially dissolved. This surface rehardens as a cellulosic film, and when dry it is permanently crisp and transparent. After the acid treatment, the cloth is neutralized in a weak alkali, washed, calendered to improve surface gloss, and perhaps mercerized again to improve transparency. This all over treatment produces organdie fabric.

In localized parchmentizing, if the design is a small figure with a large transparent area, an acid resistant substance is printed on the fabric is run through the acid bath. The acid resistant areas retain their original opacity and contrast sharply with the transparent background. If a small transparent design is desired, the acid is printed on in a paste form and then quickly washed off.

BURNED-OUT

Burned – out effects are produced by printing a chemical solvent on a blend fabric made of fibers from different groups, such as rayon and polyester. One fiber, usually the less expensive or more easily dissolved fiber, is dissolved, leaving sheer areas. The rayon has been dissolved by acid. This finish is also known as etched or devord because part of the fibers are removed by this subtractive finish.

SIZING

In sizing, or starching, the fabric is immersed in a mixture containing waxes, oils, glycerine, and softners to add or control fabric body. For added weight, talc, clay, or chalk may be used, but these are often used with lower quality fabrics. Gelatine is used on rayon because it is clear substances that enhances the natural luster of the fibers. Sizings add stiffness, weight and body to the fabric. Its permanence is related to the type of sizing is resin based and heat- set, it will be permanent. If the sizing is water soluble, it will be removed during washing or it may create problems for consumers. Geltain, for example, may create water spots on rayon if condensation or other water drops on to the fabric. These spots are difficult to remove.

WEIGHTING

Weighting is another technique used to add weight and body to a fabric. A metallic salt such as stannic chloride is used. Salts that bound with the fiber are durable; others produce temporary surface coating. Weighted silk was common once but is rare today. Weighted silk are sensitive to light damage and do not age well.

TEXTURE FINISH

SHEARED

A sheared fabric is a pile or napped fabric in which the surface has been cut to remove loose fiber or yarn ends, knots, and similar irregularities or surface flaws. Shearing is a finishing process done by a machine similar to a lawn mower to control the length of the pile or nap. It may create a smooth surface or a patterned or sculptured effect by flattening portions of the pile with an engraved roller, shearing off the areas that remain erect, and steaming the fabric to raise the flattened and now taller portions. Most pile fabrics and many napped fabrics, including cut- pile carpet, are sheared.

BRUSHED

After shearing, the fabric surface usually is brushed to clean off the fiber ends. When brushing is combined with steaming, the nap or pile is set so that it slants in one direction, producing an up and down direction for pile and nap fabrics such as corduroy.

EMBOSSED

Embossed fabrics are created using an embossing calendar that produces either flat or raised designs on the fabric. Embossing became a more important finish with the development of the heat sensitive fibers because it becomes possible to produce a durable, washable embossed pattern. Fabric made of solution dyed fabrics can be embossed directly off the loom and sold.

The embossing calendar consists of a heated, hollow engraved metal roll and a solid paper roll twice the size of the engraved roll. The fabric is drawn between the two rollers and is embossed with the design. Embossing can be done to both flat and pile fabrics.

The process differs for the production of flat and raised designs. Flat embossed designs are the simplest to produce. A metal, foam, or plastic roll engraved in deep relief revolves against a smooth paper roll. The hot engraved areas of the roll produce a glazed pattern on the fabric . embossed brocades are an example of this type of design. The effect can be seen as a difference in luster, but the fabric’s texture does not change.

PLISSE

Plisse is converted from either lawn or printed cloth gray goods by printing sodium hydroxide (caustic soda) onto the fabric in the form of stripes of designs. The alkali shrinks the fabric in the treated areas. As this shrinkage occurs, the untreated strips pucker. Shrinkage causes a slight difference in count between the two strips. The treated or flat stripe is denser. The upper portion of the fabric (figure) shows the fabric before finishing, and the lower portion shows the crinkle produced by the caustic soda treatment. This piece of goods is defective because the roller failed to print the chemical in the upper area.

The crinkle stripes can be narrow or wide. In piece- dyed fabrics, the flat treated area may be deeper colour than the puckered area. The texture change is permanent but can be flattened somewhat by steam and pressure. Plisse and embossed fabrics can be similar in appearance.

PLEATED

A pleated fabric is made using a variation of embossing. Pleating is a highly specialized operation done by either the paper pattern technique or the machine process.

The paper- pattern techniques is a more costly hand process, but it produces a wide variety of pleated designs. Partially completed garment components, such as hemmed skirt panels, are placed in a pattern mold by hand. Another pattern mold is placed on top so that the fabric is pleated between the pleating papers. The three layers are rolled into a cone shape, sealed, and heat set in a curing oven.

The machine pleating process is less expensive. High precision blades pleat the fabric as it is inserted between two heated rolls in the machine. A paper backing is used under the pleated fabric, and paper tape holds the pleats in place. After leaving the heated- roll machine, the pleats in place produces permanent three- dimensional effects in apparel, upholstery, wall coverings, window treatments, and lampshades. Pleated fabric without stitching is used in similar products, but the pleats soften with use.

FLOCKED

In a flocked fabric, a fine natural or synthetic surface fiber is applied after a base fabric has been produced. Flocking can be localized to imitate extra yarn weave or all over to imitate pile fabrics. When flocking is localized, only small areas of the fabric appear to have pile yarns, but the imitation pile is applied to the surface. An adhesive holds the very short, straight fibers in place. Area flocking can be done using either mechanical or electrostatic methods.

FULLED

Fulling is performed on wool fabrics to improve their appearance, hand , thickness, softness, body, and cover. Fabrics are fulled by moisture, heat, and friction in a very mild, carefully controlled felting process. Fulled fabric is denser and more compact in both warp and filling direction. Almost all woven wool fabrics and many knit wool fabrics are fulled. Some are lightly fulled while others are heavily fulled. Boiled wool is an example of a heavily fulled jersery.

EMBROIDERED

Embroidered fabrics are decorated by hand or by machine with a surface applied thread. Machine embroidery uses compact zigzag stitches of various lengths. Two machines are used for embroidery: the shuttle and the Multihead. The shuttle embroidery machine produces all over embroidery fabrics such as eyelet. Schiffli embroidery describes earlier machines that used punched cardboard rolls to produce all over embroidered fabrics. Contemporary shuttle embroidery machines use computers to control the pattern.

Multihead embroidery creates flat embroidery or pile embroidery. They are called Multihead because several machines are operated by the same computer system simultaneously. Multihead machines are extremely versatile and can work with a variety of threads, ribbons, or bead/ sequin strands. They can incorporate one or more colours of threads to create elaborate or simple designs in small or large scale. They create designs and emblems that are sewn to products such as leather jackets , hats , and shirts, or they are used to stitch crests, logos, and other designs on finished items.

Embroidered figures are very durable, often outlasting the ground fabric. The fabric is more expensive than the same fabric unembroidered. Like other applied designs, the figure may or may not be on grain.

Eyelet is an embroidery fabric with small round holes cut in the fabric, with stitching completely around the holes. The closeness and amount of stitching, as well as the quality of the background fabric, very tremendously.

NAPPED

Nap is a layer of fiber ends raised from the ground weave of the fabric by mechanical brushing action. Thus, napped fabrics are literally “made” by a finishing process.

Napping was a originally a hand operation using several teasels or dired plant burrs to gently brush up fiber ends. Napping is less expensive than many other ways of producing a three dimensional fabric. Napping is done by pile roller covered by a heavy fabric in which bent wires are embedded. Napping machine may be single action or double action. Fewer rollers are used in the single action machine. The bent wire ends point in the direction in which fabric travels, but the identical rollers are all mounted on a large drum or cylinder that rotates in the same direction as the fabric. The pile rolls must travel fater then the fabric to do any napping.

In the double action napping machine, every other roll is a counter pile roll, with wires that point in the direction opposite that of the pile roll. The counterpile  roll travels more slowly then the fabric to produce a nap. When the pile rolls at the slower speed and counterpile rolls at a faster speed, a “tucking” action occurs, in which the raised fibers are pushed back into the fabric, making a smooth surface.

Napping produces a fabric with appealing characteristics. A napped surface combined with soft twist filling yarns increases the air volume. The fabric is soft and attractive and is good insulator. A dense mat of fiber end on the surface imparts a degree of water repellency.

Note :   Wool napped fabrics is called as flanned.