TEXTILE SCIENCE -I

UNIT - I

Introduction to the field of Textiles – major goals – classification of fibers –

Natural & chemical – primary and secondary characteristics of textile fibers

AIM AND OBJECTIVES

- The history of clothing and textiles

- Origin of Indian textiles

- Textile industry and significant changes

- Scope of textile

- classification of textile fibers & there properties

INTRODUCTION

A textile is a flexible material comprised of a network of natural or artificial fibers often referred to as thread or yarn. Textiles are formed by weaving, knitting, crocheting, knotting, or pressing fibers together (felt).

Textiles are classified according to their component and structure or weave. Value or quality in textiles depends on several factors, such as the quality of the raw material used and the character of the yarn spun from the fibers, whether clean, smooth, fine, or coarse and whether hard, soft, or medium twisted.

Yarn, fabrics, and tools for spinning and weaving have been found among the earliest relics of human habitations. The Textile industry is a term used for industries primarily concerned with the design or manufacture of clothing as well as the distribution and use of textiles.

THE FIELD OF TEXTILE

Food, shelter and clothing are the basic needs of everyone. All clothing is made from textile and shelters are made more comfortable and attractive by the use of textiles. Everyone is surrounded by textiles from birth to death. We walk on and wear textile products; we sit on fabric covered chairs and sofas; we sleep on and under fabrics; textiles dry us or keep us; they keep us warm and product from sun, tire, and infection. Clothing and household textiles are aesthetically pleasing and vary in colour, design and texture. They are available in a variety of

Price ranges. The history of clothing and textiles attempts an objective survey of clothing and

textiles throughout human history, identifying materials, tools, techniques, and influences, and the cultural significance of these items to the people who used them. Textiles, defined as felt or spun fibers made into yarn and subsequently netted, looped, knit or woven to make fabrics, appeared in the Middle East during the late stone age.[1] From ancient times to the present day, methods of textile production have continually evolved, and the choices of textiles available have

Influenced how people carried their possessions, clothed themselves, and decorated their surroundings.

Yarn, fabrics, and tools for spinning and weaving have been found among the

Earliest relics of human habitations. Linen fabrics dating from 5000 B.C. have

been discovered in Egypt. Woolen textiles from the early Bronze Age in

Scandinavia and Switzerland have also been found. Cotton has been spun and

Woven in India since 3000 B.C., and silk has been woven in China since at least

1000 B.C. about the 4th cent. A.D., Constantinople began to weave the raw silk

Imported from China.

India has a diverse and rich textile tradition. The origin of Indian textiles can be

Traced to the Indus valley civilization. The people of this civilization used homespun cotton for weaving their garments. Excavations at Harappa androgen -jo-Daro, have unearthed household items like needles made of bone and spindles made of wood, amply suggesting that homespun cotton was used to make garments.

1500 A.D. spinning was done entirely by hand. Spinning by hand was cumbersome, tedious and a very slow process indeed. Men and women too began to look around for a more satisfactory method of weaving threads together into cloth. At the beginning of the sixteenth century, a one-thread machine was invented which was a tremendous stride ahead of the old by-hand methods. It enabled the spinner to produce about seven times more yarn than by the distaff and spindle. New improvements and new inventions were gradually made, until the making of cloth was taken entirely out of the hands of the women in the homes and spinning was relegated into the realms of the "old-fashioned."

During the industrial revolution, production was mechanized with machines powered by waterwheels and engines. Sewing machines emerged in the nineteenth century. Synthetic fibers such as nylon were invented during the twentieth century. Alongside these developments were changes in the types and style of clothing worn by humans. During the 1960s, had a major influence on subsequent developments in the industry.

The textile industry has undergone significant changes in business practices in several key areas. Labor relations, trade practices, product labeling, product safety, and environmental and antipollution measures have been subjects of public scrutiny and federal legislation.

The words fabric and cloth are commonly used in textile assembly trades (such as tailoring and dressmaking) as synonyms for textile. However, there are subtle differences in these terms. Textile refers to any material made of interlacing fibres. Fabric refers to any material made through weaving, knitting, crocheting, or bonding. Cloth refers to a finished piece of fabric that can be used for purpose such as covering a bed.

MAJOR GOALS

Textile production played a crucial part in the industrial revolution, the establishment of organized labor, and the technological development of the country. Once, textile production was simple enough that the entire process could and did take place in the home. Now, textiles represent a complex network of interrelated industries that produce fiber, spin yarns, fabricate cloth, and dye, finish, print, and manufacture goods. A material made mainly of natural or

Synthetic fibers. They are found in apparel, household and commercial furnishings, vehicles, and industrial products.

Textiles have an assortment of uses, the most common of which are for clothing and containers such as bags and baskets. In the household, they are used in carpeting, upholstered furnishings, window shades, towels, covering for tables, beds, and other flat surfaces, and in art. In the workplace, they are used in industrial and scientific processes such as filtering.

Miscellaneous uses include flags, tents, nets, cleaning devices, such as hand kerchiefs; transportation devices such as balloons, kites, sails, and parachutes; strengthening in composite materials such as fibre glass and industrial geo textiles, and smaller cloths are used in washing by "soaping up “the cloth and washing with it rather than using just soap.

Textiles used for industrial purposes, and chosen for characteristics other than their appearance, are commonly referred to as technical textiles. Technical textiles include textile structures for automotive applications, medical textiles(e.g. implants), geo textiles (reinforcement of embankments), agro textiles (textiles for crop protection), protective clothing (e.g. against heat and radiation for firefighter clothing, against molten metals for welders, stab protection, and bulletproof vests. In all these applications stringent performance requirements must be met.

PRODUCTION METHODS

There is a logical development of raw material into finished consumers' goods. Studying textile materials in the interesting sequence of "fiber to yarn to fabric" will help understand the construction and ultimate qualities of the fabrics with which will become familiar. Here are the steps in the manufacture of fabrics from raw material to finished goods:

Spinning

The fabrication of yarn (thread) from either discontinuous natural fibers or bulk synthetic polymeric material. In a textile context the term spinning is applied to two different processes leading to the yarns used to make threads, cords, ropes, or woven or knitted textile products.

Weaving

Weaving is a textile production method which involves interlacing a set of vertical threads (called the warp) with a set of horizontal threads (called the weft). This is done on a machine known as a loom, of which there are a number of types. Some weaving is still done by hand, but the vast majority is mechanized.

Knitting

Knitting and crocheting involve interlacing loops of yarn, which are formed either on a knitting needle or on a crochet hook, together in a line. The two processes are different in that knitting has several active loops at one time, on the knitting needle waiting to interlock with another loop, while crocheting never has more than one active loop on the needle.

Braiding

Braiding or plaiting involves twisting threads together into cloth. Knotting

Involves tying threads together and is used in making macramé.

Lace

Lace is made by interlocking threads together independently, using a backing

and any of the methods described above, to create a fine fabric with open holes

in the work. Lace can be made by either hand or machine.

Felting

Felting involves pressing a mat of fibers together, and working them together

until they become tangled. A liquid, such as soapy water, is usually added to

lubricate the fibers, and to open up the microscopic scales on strands of wool.

• Carpets, rugs, velvet, velour, and velveteen, are made by interlacing a

secondary yarn through woven cloth, creating a tufted layer known as a nap or

pile.

FIBRES

Fibre, fine hair-like structure of animal, vegetable, mineral, or synthetic origin. Fibres average less than 0.05 cm (0.02 in) in diameter. Used for textiles and for many other products, fibres are classified according to their origin, their chemical structure, or both.

The first essential of a fibre is that it must be hundreds of tines longer than it is wide to enable it to be spun into a thread for weaving. It must also be strong and flexible and elastic enough to withstand the strain of the processes required to produce a cloth that wears well. If the fibre is a very coarse one, it produces a cloth resembling sacking. For comfort in weaving, all fibres need to be able to absorb moisture. Luster may be desirable for appearance, and weight and flexibility can affect draping.

The basic unit of a textile structure is fibre. The textile industry uses many different kinds of fibres as its raw materials. Some of these fibres were known and used in the earlier years of civilization, as well as in modem times.

Fibre is a class of hair-like materials that are continuous filaments or are indiscrete elongated pieces, similar to pieces of thread. They can be spun into filaments, thread, or rope. They can be used as a component of composite materials. They can also be matted into sheets to make products such as paper or felt.

CLASSIFICATION OF FIBRES

In order to simplify the study of textile fibres, materials with similar properties must be grouped in some logical order. Each country has developed its own system for naming fibres. The two major groups, or families, of fibres specified by the act are:

- Natural fiber and

- Man made or synthetic fiber.

NATURAL FIBERS

The term “natural fibers” covers a broad range of vegetable, animal, and mineral fibers Vegetable fibers

Vegetable fibers are generally comprised mainly of cellulose: examples include cotton, linen, jute, flax, ramie, sisal, and hemp. Cellulose fibers serve in the manufacture of paper and cloth.

This fiber can be further categorized into the following:

• Seed fiber: Fibers collected from seeds or seed cases. E.g. cotton and kapok.

• Leaf fiber: Fibers collected from leaves. E.g. sisal and agaves.

• Bast fiber or skin fiber: Fibers are collected from the skin or bast surrounding the stem of their respective plant. These fibers have higher tensile strength than other fibers. Therefore, these fibers are used for durable yarn, fabric, packaging, and paper. Some examples are flax, jute,

kenaf, industrial hemp, ramie, rattan, soybean fiber, and even vine fibers and banana fibers.

• Fruit fiber: Fibers are collected from the fruit of the plant, e.g. coconut (coir) fiber.

• Stalk fiber: Fibers are actually the stalks of the plant. E.g. straws of wheat, rice, barley, and other crops including bamboo and grass. Tree wood is also such a fiber. The most used natural fibers are cotton, flax and hemp, although sisal, jute,kenaf, and coconut are also widely used. Hemp fibers are mainly used for ropes and aerofoil because of their high suppleness and resistance within an aggressive environment. Hemp fibers are, for example, currently used as a seal within the heating and sanitary industries.

ANIMAL FIBERS

Animal fibers generally comprise proteins and are commonly made from hair or fur.

• Wool refers to the hair of the domestic goat or sheep, which is distinguished from other types of animal hair in that the individual strands are coated with scales and tightly crimped, and the wool as a whole is coated with an oil known as lanolin, which is waterproof and dirt proof. Woolen refers to a bulkier yarn produced from carded, non-parallel fibre, while worsted refers to a finer yarn which is spun from longer fibres which have been combed to be parallel. Wool is commonly used for warm clothing.

Cashmere, the hair of the Indian Cashmere goat, and mohair, the hair of the North African Angora goat, are types of wool known for their softness. Other animal textiles which are made from hair or fur are alpaca wool, l lama wool, and camel hair, generally used in the production of coats, jackets, ponchos, blankets, and other warm coverings. Angora refers to the long, thick, soft hair of the Angora rabbit.

• Silk is an animal textile made from the fibers of the cocoon of the Chinese silkworm. This is spun into a smooth, shiny fabric prized for its sleek texture.

MINERAL FIBERS

Mineral fibers are naturally occurring fiber or slightly modified fiber procured from minerals. These can be categorized into the following categories:

• Asbestos and basalt fiber are used for vinyl tiles, sheeting, and adhesives," transit" panels and siding, acoustical ceilings, stage curtains, and fire blankets.

• Glass Fiber is used in the production of spacesuits, ironing board and mattress covers, ropes and cables, reinforcement fiber for composite materials, insect netting, flame-retardant and protective fabric, sound proof, fireproof, and insulating fibers.

• Metal fiber, metal foil, and metal wire have a variety of uses, including the production of cloth-of-gold and jewelry. Hardware cloth is a coarse weave of steel wire, used in construction.

MAN MADE FIBRES

Synthetic fibers are the result of extensive research by scientists to improve upon naturally occurring animal and In general, synthetic (manmade) fibers are created by forcing, usually through extrusion, fiber forming materials through holes (called spinnerets) into the air, forming a thread. Before synthetic fibers were developed, artificial (manufactured) fibers were made from cellulose, which comes from plants.

The manufacturing process of regenerated fibres consists of bringing a natural high polymer substance into solution in a suitable way and extruding this solution through a nozzle (orifice), regenerating the same high polymer in the form of a solid filament. A regenerated fibre is one which has a different physical structure than the substance from which it is made, but is essentially the same chemically. Rayon is Regenerated Cellulose, i.e., cellulose that has gone through the manufacturing process, from solid to liquid to solid, without chemical change.

The first artificial fiber, known as artificial silk from 1855 onwards, became known as viscose around 1894, and finally rayon in 1924. A similar product known as cellulose acetate was discovered in 1865. Rayon and acetate are both artificial fibers, but not truly synthetic, being made from wood. Although these artificial fibers were discovered in the mid-nineteenth century, successful modern manufacture began much later Nylon, the first synthetic fiber, made its debut in the United States as are placement for silk, just in time for World War II rationing. Its novel use as a material for women's stockings overshadowed more practical uses, such as are placement for the silk in parachutes and other military uses. Common synthetic fibers include:

• Polyester fiber is used in all types of clothing, either alone or blended withfibres such as cotton.

• Aramid fiber (e.g. Twaron) is used for flame-retardant clothing, cut protection,and armor.

• Acrylic is a fibre used to imitate wools, including cashmere, and is often used in replacement of them.

• Nylon is a fibre used to imitate silk; it is used in the production ofpantyhose. Thicker nylon fibers are used in rope and outdoor clothing.

• Spandex (trade name Lycra) is a polyurethane fibre that stretches easily and can be made tight-fitting without impeding movement. It is used to make active wear, bras, and swimsuits.

• Olefin fiber is a fiber used in active wear, linings, and warm clothing. Olefins are hydrophobic, allowing them to dry quickly. A sintered felt of olefin fibers is sold under the trade name Tyvek.

• Ingeo is a polylactide fiber blended with other fibres such as cotton and used in clothing. It is more hydrophilic than most other synthetics, allowing it to wick away perspiration.

• Lurex is a metallic fiber used in clothing embellishment.

PROPERTIES OF SYNTHETIC FIBRES.

They are flexible, light and very resistant. They do not absorb humidity and maintain body heat, therefore they are not suitable for the manufacture ofs ummer articles if not mixed with other natural fibres. They do not shrink, crease and maintain machine pleating, avoiding ironing. They dye well. Due to their elasticity they are used in the manufacture of underwear, swimming costumes and sportswear

FIBRE PROPERTIES

To be spinnable, a fibre must have sufficient length, pliability, strength, and cohesiveness to form a yarn. Fibres must also be inexpensive, available, and constant in supply to be economically suitable for production. To make such afabric the manufacturer chooses fibres, yarns, weaves, and finishes with acombination of properties which will give the type of

Serviceability the consumer wants.

PRIMARY CHARACTERISTICS OF TEXTILE FIBRE

The primary properties of textile fibre is

• Stable length

• Tensile strength,

• Fineness,

• Spinnability, and

• Uniformity

Stable length - Staple fibres are short in length, measured in inches and range from three-quartos of an inch to 18 inches in length. All the natural fibres, except silk, are staple fibres. Any filament fibre can be cut into staple of length determined by the end-use desired.

Tensile strength - Strength of a fibre is the ability to resist strains and stresses. It is expressed as tensile strength which is measured in pounds per square inch (p.s.i.) or as tenacity which is measured in grams per denier. Some fibres gain strength when wet, some lose strength, and some are unaffected by water.

Fineness – In a fibre, the ratio or relationship if length to width or cross sectional area is expressed as its fineness. In coarse fibres the length is about700 times more than the width. The ratio may be even 5000 in case of very fine fibres. Only fine fibres can produce fine yarn. Fineness does much to determine properties and characteristics of particular fibre and it also determines the end use of fibres.

Spinnability – Spin ability includes several physical properties each having an

effect on the ability of the fibres to be spun into yarn. For Example: Staple fibres must have to be capable of taking a twist. They must have a certain degree of friction against one another to stay in place when pull is applied to the yarn. And they must be able to take on hole special finishes for lubrication during spinning or to provide additional surface resistance to abrasion.

Uniformity –This means the evenness of the individual fibres in length and diameter. A fibre possessing this property can produce reasonably even threads. This is also important in connection with the strength of the resulting yarn. The more uniform the yarn the stronger the yarn.

SECONDARY CHARACTERISTICS OF TEXTILE FIBRE

The secondary properties of textile fibre is

• Crimp

• Elasticity

• Cohesion

• Density

• Plasticity

• Absorbency

• Resilience

• Capillarity or Porosity

• Colour

• Luster

• Flexibility

• Rigidity

• Abrasion resistance

• Static electric resistance

Crimp - Crimp refers to the waves or bends that occur along the length of a fibre. Wool has natural crimp. Manmade fibres may be given a permanent crimp. Fibre crimp increases cohesiveness, resiliency, and resistance to abrasion. Ithelps fabrics maintain their thickness.

Elasticity - Elasticity means the ability of a stretched material to return immediately to its original size.

Cohesion - Cohesiveness is the ability of fibres to cling together. This is important in staple fibres, but unimportant in filament fibres.

Density - Density and specific gravity are measured of the weight of a fiber. Density is the weight in grams per cubic centimeter. Specific gravity is the ratio of the mass of the fibre to the mass of an equal volume of water at 40°C. The weight of a fabric is determined by the density or specific gravity of the fibres.

Plasticity - Plasticity is that property of a fibre which enables the user to 'shape it semi-permanently or permanently by moisture, heat, and pressure or by heat and pressure alone.

Absorbency - Absorbency is the ability of a fibre to take up moisture and is expressed as percentage of moisture regain, which is the percentage of moisture that a bone-dry fibre will absorb from the air under standard conditions of temperature and humidity. The ability of a fibre to absorb moisture is directly related to wash ability, dyeing, shrinkage, absorption of aqueous finishes, comfort on humid days, and soiling. Staple fibres hold more water than filament

fibres since they pack less compactly and create a sponge-like condition in the yarn and fabric. For this reason staple fibre fabrics require a longer drying time.

Resilience - Resiliency is the ability of a fibre or fabric to recover, over a period of time, from deformation such as stretching, compressing, bending or twisting. A resilient fabric has good crease recovery, hence requires a minimum of ironing. Resilient fabrics also retain high bulk.

Capillarity or Porosity - This two terms express properties with the similar influence on the ability of a textile fibre or yarn to accept and hold a dye, a finish a lubricant or even resin in order to increase the wrinkle resistance of a fabric or to give it a wash and wear finish. Liquids passed rapidly through porosity. In the case of the passage of these liquids through the hollow centre or lumen in cotton or through small voids on the surface of wool fibre. It is usually regarded as the effect of the mechanism capillarity.

Colour – Most natural fibre have some colour. The synthetic fibres too have a

slight creamy or yellow colour.

For Example:

Silk is yellow to tan

Wool is brownish tint

Cotton is a creamy white or brown

Luster - Luster is the shine, sheen or brightness of a fibre caused by reflection of light. Smooth fibres reflect more light than rough or serrated fibres; round fibres reflect more light than flat fibres. Filaments which are laid together with little or no twist reflect more light than short fibres which must be twisted together to forth yarns. Manmade fibres can be de lustered by adding oil or

Pigments to the solution from which the fibre is spun.

Flexibility - Pliability or flexibility is the ease of bending or shaping. Pliable fibres are easily twisted to make yarns. They make fabrics that resist splitting when folded or creases many times in the same place.

Rigidity - Stiffness or rigidity is the opposite of flexibility. It is the resistance to bending or creasing. Rigidity and weight together make up the body of the fabric.

Abrasion resistance - Abrasion resistance is the ability of a fibre to with stand the rubbing or abrasion it gets in everyday use. Inherent toughness, natural pliability, and smooth filament surface are fibre characteristics that contribute to abrasion resistance.

Static electric resistance - Phenomenon of static electricity creates a problem in the spinning and other processing of textile fibres especially in rooms with very low relative humidity. The problem is much more severe in the case of synthetic fibres which have extremely low electrical conductivity and generally absorb too little moisture to provide a path where y the static electricity can be carried away. Static electrical properties create problems in the packaging and in the sewing

Other Characteristics of Textile Fibre

• Wicking or wetting

• Chemical resistance

• Resistance to moths, and mildew

• Flammability or inflammability

Wicking or wetting - Wicking or wetting refers to the conduction of moisture along the fibre or through the fabric, although the fibre itself does not absorb much moisture. This property is related to surface wetting and is not the same as absorbency.

Chemical resistance - The chemical reactivity of each fibre depends on the arrangement of the elements in the molecule and the reactive groups it contains. Dry-cleaning solvents, perspiration, soap, synthetic detergents, bleaches, atmospheric gas, soot, and sunshine may all cause chemical degradation on some or all of the fibres.

Resistance to moths, and mildew - Resistance to moths, and mildew is due to the chemical composition of the fibre. These properties are important to the consumer because they indicate the type of care needed during storage as well as during use. Fibres without natural resistance must have protective finishes added or have their chemical composition changed to make them resistant.

Flammability or inflammability - Flammability or inflammability refers to the ease of ignition and the speed and length of burning. Non-flammable fibres will not burn. Flammability depends not only on the chemical composition but on the air incorporated in the yarn or fabric. Combustible finishes or dyes may take a non-flammable fibre burn. Finishes can also be added to make fibres nonflammable.

Cotton

Cotton is obtained plant source and it is classified as a natural material as it

is obtained from the seeds of cellulose seed fibre staple fibre measuring 10-

65mm in length and white to beige in color in its natural state. It is composed

Basically of a substance called cellulose. As cotton occupies 50% of the

Consumption of fibres by weight in the world it is called as the king of all fibres.

Cotton is the fabric for every home and is the most widely produced of

Textile fabrics today. It has now been proved that India was the first country to

Manufacture cotton. Among the recent findings at Mohenjo-Daro were a few

scrapes of cotton sticking to the side of a slivers vase. Cotton is the white downy

Covering of the seed grown in the pods. The cotton plant grown in the tropics

needs a climate with 6 months of summer weather to blossom and produce

pods.

The cotton fibre is the shortest of all the textile fibres. Its length varies from

8/10 of an inch to 2 inches. Cotton with short length fibres is technically known

as “short staple”. The one with the long fibres is called “long staple” and it more

used since it is used for making fine qualities of cloth. Long staple is especially

suitable as it is easy to spin and produces a strong smooth yarn. It is also suitable

for mercerization a finishing process used to improve the absorbency, strength

and luster of fibre.

Cultivation of cotton

The principal cotton producing regions are Egypt, southern United States,

India, Brazil the western and southern cost of America and East Indies. It requires

200 days to continue warm weather with adequate moisture and sunlight. Frost

is harmful to the plant. March and April months are suitable for plantation.

America produces more than 40% of the world’s cotton. India ranks second

to the United States as a producer and exporter of cotton.

Manufacture of Machine made cotton

Cotton pods

↓

Ginning (Removal of Seeds)

↓

Lap Formation

↓

Carding

↓

Doubling --> Combing

↓

Drawing

↓

Roving

↓

Spinning

Preparation: The fibres are first removed from seeds in a gin. This process

is called ginning. Every bit of the cotton fibre is used in the manufacture . The

fibre mass is then compressed into bales and shipped into spinning mills.

The short ends left on the seeds after the longer fabric. Fibres have been

removed are used in the production of rayon, plastics, dynamite and many

other by products, which are then used in the production of seed oil, hydrogenated

fats, soaps and cosmetics.

Forming the laps: In the step dirt from cotton fibre is removed and fibres

are made in to a soft roll or lap. Then several laps are combined into one.

Carding: These fibres are drawn together to form a loose rope called

sliver.

Doubling: Slivers are combined here for uniformity.

Combing: This process is continuation and refinement of carding process.

All cotton yarns for fabrics are carded but not all are combed. Yarns that are

combed are finer even and free from all woody stalk of the plant. They are used

for finer quality fabrics such as voile and organdie. Fabrics made from these

fabrics are expensive too. The slivers are called carded slivers.

Drawing: The slivers is then combined, smoothened and stretched. The

slivers may be drawn reduced further in size and given a slight twist by a process

called roving in which the slivers is passed through rollers and wound on to

bobbins set into spindles. It is done in a speed frame.

Roving: The bobbins are placed on the roving frame where further drawing

and twisting takes place until the cotton stock is about a pencil lead in diameter.

Spinning: Done on the spinning frame where the stock passes through sets

of high speed rollers and gives the yarn of desired thickness.

Weaving and dying: The yarn is then knitted or woven in any one of the

variety of weaves and structures. Warp yarns are usually more strongly twisted

than filling yarns since they must withstand greater strain in weaving and finishing.

Dye stuffs may be applied to raw cotton, yarn or piece goods.

Finishing: It includes starching, calendaring, sanforizing,mercerizing or other

finishes as it is necessary for the particulars use for which the cloth is intended.

These finishes may be applied to yarns but are usually applied to fabric. The

fabrics may be given these special finishes before or after dyeing.

Physical properties

a. Structure: The cotton fibre is short (1/2 inch -2 long inch) and cylindrical

or tubular as it grows. The cotton fibre is essentially cellulose consisting of carbon,

hydrogen and oxygen. Bleached cotton is almost pure cellulose raw cotton

contains about 5% of impurities.

b. Strength: Cotton fibre is relatively strong which is due to the intricate

structure and 70% crystalline.

c. Elasticity: Cotton is relatively inelastic because of its crystalline polymer

system and for this reason cotton textile wrinkle and crease readily.

d. Hygroscopic moisture: Cotton does not hold moisture so well as wool

or silk but absorbs it and so feels damp much more quickly. It also rapidly

spreads throughout the material.

e. Electrical property: The hygroscopic nature ordinarily prevents cotton

textile materials from developing static electricity.

f. Absorbency: As cotton has cellulose it is a good absorbent of fibre.

2. Thermal properties

Cotton fibres have the ability to conduct heat energy, minimizing any

destructive heat accumulation thus they can withstand hot ironing temperature.

Drap ability: Cotton does not have good body to drape well in shape.

The type of construction of the fabric may improve this property.

Resilience: Cotton wrinkles easily some wrinkle resistant finishes may

reduce this property.

Cleanliness and wash ability: Though cotton absorbs dust due to its

rough nature. It can be washed easily in the hot water and strong soaps without

damaging the fibre.

Luster: The natural cotton has no pronounced luster. This can be improved

by the mercerization finish of the cotton(that is sodium hydroxide treatment).

Shrinkage: The fibre itself does not shrink but cotton fibre which has been

stretched in the finishing process tends to relax back creating shrinkage.

Heat conductivity: Cotton is the better conductor of heat than wool or

silk but not as good as rayon.

3. Chemical properties

Action of acids and alkalies

Strong acids will destroy the fibres immediately. Dilute inorganic acids will

weaken the fibre and if left dry will rot it. Therefore after treatment with acidic

solutions cotton articles should be thoroughly rinsed in water. They are affected

very little by organic acids. They are also quite resistant to alkalis even to strong

caustic alkalies at high temperature and pressure.

In 8% NaOH cotton fibres swells, spirals, twisted uncoil and shrinks and

become thicker. The resultant fibre is smoother, lustrous, and stronger and has

increased water and dye absorption.

Effect of bleaching: These have no effects until used in uncontrolled

conditions and with heat.

Effect of sunlight and weather: Ultraviolet rays of sunlight affect the

strength of fibre and change the colour to yellow when exposed to prolonged

period. Pollution also effect fibre. Concentrated and diluted mineral acids like

sulphuric acids will discolor fibre .

Affinity to dyes: Cotton takes in dyes better than linen but not as readily

as silk and wool. If a mordant is used cotton is easy enough to dye mordant

colours, direct or substantive dyes should be applied to the cotton.

Effect of perspiration: Both acidic and alkaline perspiration discolors

the fibre.

Biological properties

Resistance to micro organisms: The mildew and bacteria damages cotton.

Resistance to insects: Moths and beetles will not affect or damage the

cotton. But the sliver fish eats the cotton cellulose.

Major end uses

Cotton is used for home furnishing : Towels are most common as it is

high in absorbency, wide range of colors, wash ability and durability. Sheets and

pillow cases are mostly blends of cotton with polyester or made of pure cotton.

Drapes, curtains and upholstery fabrics are made of cotton and its blends.

Since cotton can be autoclaved at high temperatures, absorbency,

wash ability and low static build up are important factors for use of cotton in

hospitals.

Industrial uses include book bindings, luggage’s, and hand bags, shoes and,

slippers, tobacco cloth, woven wiping cloths as and wall covering fabrics.

Wide range of wearing apparels: blouses, shirts, dresses, children wear,

active wear, separates swimwear, suits, jackets, skirts, pants, sweaters, hosiery,

bedspreads, comforters, throws, sheets, towels, table cloths, table mats, napkins.

SILK:

Introduction

Silk is considered as “Queen of all textile fibres” as it has beauty and elegance

and good properties of performance. Silk is the natural protein fiber obtained

from silk worm cocoons. Japan is known for producing best variety of silk.

India produces different varieties of silk and is famous for hand woven silk

textiles. There is a tremendous silk production increase in recent years. The

production of silk is called Sericulture. To obtain quality and quantity of silk

rearing conditions are controlled carefully throughout the life cycle of silk moth.

These are two types of silk mulberry or cultivated silk and wild silk.

Cultivated silk is creamy silk white or yellowish white in color. White wild silk

color range from brownish to golden yellow in color.

History of silk

Sericulture or silk production has a long and colorful history unknown to

most people. For centuries the west knew very little about silk and people who

made it pliny, the roman historian wrote in his natural history in 70 BC “silk was

obtained by removing the down from leaves with the help of water”. For more

than 2000 years these Chinese kept the secret of silk altogether to themselves.

According to legend the beginning of history of use of silk as textile fibre goes

back to 260 BC. When fourteen year old wife of Chinese emperor Huang-Ti

discovered the secret of drawing the filament from cocoon of the silk worm and

producing a fabric from the filament. This young princess Si-ling-chi is known as

‘goddess of silk worms’ and is the centre of religious ceremonies connected with

the care of silk worms and the production of silk has long been an important

factor in economy of empire.

Silk has never lost its luxury field appeal and today is shown by all houses

in their top fashion products some designers are working only on silk. It is

everywhere in fashion picture. In intimate wear and outer wear, hand bags and

shoes.

Production of Silk

Silk worms feed on mulberry tree leaves and therefore for rearing them,

the growing of mulberry trees is the first essential step. These are grown by the

agriculturists.

Silk worms have a short life of only about two months and during which

these pass through the following four stages1. Egg 2.worm or larvae 3. Pupa

and 4. moths.

Silk worms are made to lay eggs on specially prepared paper for this

purpose.

Silk moth and eggs                                                                  Larva of Italian Bombyx

Cocoon of Bombyx mori      Male Bombyx mori or mulberry-

feeding silk worm moth

Silk worms are made to lay eggs on specially prepared paper for this

purpose. The eggs can be stored in cold storage for six weeks. Eggs are collected

and kept at low temperature until they are hatched. Eggs take ten days to hatch

Emerged caterpillars of ant head size are fed on fresh mulberry leaves. At this

stage the worm needs special care bamboo trays with straw mats are provided

for them. When the caterpillar is about eight weeks old it secretes a viscous fluid

from two glands on its head which oozes out from the common opening near its

mouth. The fluid is called ‘fibrion’.At the same time it also secretes a gummy

kind of fluid called ‘sericin’ which passes through the same opening. The fibroin

gets hardened when exposed to air. The silk worm spins around itself to form a

cocoon. The cocoon contains 2000 to 4000 yards of reelable silk. For separating

the silk thread from the cocoons they are immersed in hot water. This immersion

also kills the warm inside. Then the cocoons are dries and stored.

Reeling: The process of unwinding the filament from the cocoon is called

reeling. The care and skill in the reeling operation prevents defects in the raw

silk. As the filament of single cocoon is too fine for commercial use, three to ten

strands are usually reeled at a time to produce the desired diameter of raw silk

thread. Several cocoons are placed in hot water to soften the gum and the

surfaces are brushed lightly to find the ends the filaments. These ends are collected,

threaded through a guide and wound on to a wheel called ‘reel’.

Throwing: As the fibres are combined and pulled on to the reel, twist can

be inserted to hold the filaments together. This is called as throwing and the

resulting yarn is ‘thrown yarn’. This yarn later goes to weaving or knitting industry

based the type of yarn produced.

Spinning: Short ends of silk fibres from the outer and inner edges of the

cocoons and from broken cocoons and spun into yarns in a manner similar to

that used for cotton. This is called spun silk.

Degumming: Sericin or gum up to 30% of the weight of the silk fibre. It is

not usually removed until after the cloth is woven because serves as warp sizing

that protects the yarns from mechanical injury during weaving. Sericin remains

on the fibre during reeling and throwing before finishing, the gum is removed by

boiling the fabric in soap and water. The presence of gum and sericin increases

the tendency for the silk to water spots on fabrics when ironed.

Bleaching: Silk thread is treated with hydrogen peroxide.

Dyeing: Silk has great affinity for the dyes. Acid dyes produce brilliant

shades on silk.

Printing: Silk may be left plain or may be printed by any method like roller

printing, Screen printing or block printing. Silks are usually dried and then printed.

Finishing: Silk fabrics require very few finishes because they have natural

luster, softness and Drapability.

Weighting of silk:

When silk is boiled to remove the excess of natural

gum or sericin it looses weight. This loss of weight is replaced through treatment

by metals like tin, aluminium etc in water solutions. These are not removed by

washing.

Weighted silk is not durable because sunlight and perspiration weakens

fibres. Heavy weighting causes silk to crack.

Various types of silk

Wild silk: Silk produced by moths of species other than bombyx mori. It

is brown in color more uneven and coarser. It is usually called Tussar silk.

Waste silk or silk noil: Short ends of spun yarns or in blends with cotton

or wool. Sometimes it is called waste silk.

Dupion: Silk yarns made from two cocoons that have been formed in an

interlocked manner. The yarn is uneven, irregular and large than regular filaments.

It is used in making shantung and duppioni.

Raw silk: Silk that has not had any degumming.

Spun silk: Yarns made from short fibres from pierced cocoons and short

ends and outside and inside the edges of cocoons.

Properties of silk:

Strength: Silk is the strongest natural fibre. It has a tenacity of 2.4 to 5.1

grams per denier. More over smoothness of the silk filament yarn reduces the

problem of wear from abrasion. The strength of the spun silk yarns depends on

the length of silk staple.

Shape and appearance: Silk filaments are very fine and long. They

frequently measure about 1000 to 1300 yards in length. The width of the silk is

from 9 to 11 microns.

Elasticity: It is an elastic fibre and its elasticity varies as it is natural fibre.

Silk fibre may be stretched from 1/7 to 1/5 its original length before breaking.

Cultivated degummed silk viewed longitudinally under a microscopic,

resembles a smooth transparent rod under microscope. Silk in the gum has

rough irregular surface. Wild silk tend to be quite uneven and is some what

dark. It may have longitudinal striations.

Resilience: Silk retains the shape and resists wrinkling rather well. This is

more in fabrics made from pure silk rather than spun silk or weighted silk.

Drapability: Silk has a pliability and suppleness’ that aided by its elasticity

and resilience gives it excellent Drapability.

Heat conductivity: Since silk is a protein fibre. It is a non conductor of

heat like wool. Hence it is used for winter apparel.

Absorbency: The good absorptive property of silk also contributes to its

effect in warmer atmosphere. Silk generally absorbs about 11% of its weight in

moisture which makes silk for easy dying and printing.

Cleanliness and wash ability: Silk is hygienic material because its smooth

surface does not attract dirt. It can also be easily cleaned by mild soaps and dry

cleaning.

Shrinkage: Due to the filament in length, smooth surface silk have normal

shrinkage which can be easily restored by ironing at moderate heat and damp

conditions.

Effect of light: Continuous exposure to light weakens silk faster than either

cotton or wool.

Chemical properties

Resistance to mildew: Silk will not be affected by mildew unless left for

time in damp state or under extreme conditions of tropical dampness.

Reaction to alkalis: Silk is not as sensitive as wool to alkalis. It may be

affected in concentrations and high temperatures. Cold concentrated solutions

of alkali such as soda or caustic potash has slight action on silk. Heated solution

dissolved silk.

Reaction to acids: Concentrated mineral acids dissolve faster than wool.

Organic acids do not harm them while medium concentrated HCL will dissolve

silk.

Affinity for dyes : Silk has very good affinity for acid dyes but light fastness

is unsatisfactory.

Resistance to perspiration: Silk fabrics are damaged by perspiration.

The silk itself gets deteriorated in the presence of perspiration.

Reaction to bleach: Strong bleaches contain sodium hypochlorite will

deteriorate silk. Mild bleaches like sodium perborate and hydrogen peroxide

may be used with normal caution.

Uses of silk

Silk is an expensive luxury fabric used for making different garments. Silk is

used primarily in apparel and home furnishing items because of its appearance

and cost. Silk is extremely versatile and can be used to create a variety of

fabrics from sheer chiffons to heavy beautiful brocades and velvets. Because of

silk absorbency it is appropriate for warm weather wear. Because of its low

conductivity it is used for cold weather wear, also in furnishing silk is often blended

with other fibres to add soft luster for furnishing fabric. Occasionally expensive

hands made rugs are made from silk.

### Clothing

Silk's absorbency makes it comfortable to wear in warm weather and while active. Its low conductivity keeps warm air close to the skin during cold weather. It is often used for clothing such as shirts, ties, blouses, formal dresses, high fashion clothes, lining, lingerie, pajamas, robes, dress suits, sun dresses and Eastern folk costumes. For practical use, silk is excellent as clothing that protects from many biting insects that would ordinarily pierce clothing, such as mosquitoes and horseflies.

Fabrics that are often made from silk include charmeuse, habutai, chiffon, taffeta, crepe de chine, dupioni, noil, tussah, and shantung, among others.

### Furniture

Silk's attractive luster and drape makes it suitable for many furnishing applications. It is used for upholstery, wall coverings, window treatments (if blended with another fiber), rugs, bedding and wall hangings.

### Industry

Silk had many industrial and commercial uses, such as in parachutes, bicycle tires, comforter filling and artillery gunpowder bags.[64]

### Medicine

A special manufacturing process removes the outer sericin coating of the silk, which makes it suitable as non-absorbable surgical sutures. This process has also recently led to the introduction of specialist silk underclothing, which has been used for skin conditions including eczema. New uses and manufacturing techniques have been found for silk for making everything from disposable cups to drug delivery systems and holograms.

### Biomaterial

Silk has been considered as a luxurious textile since 3630 BC. However, it started to serve also as a biomedical material for suture in surgeries decades ago. In the past 30 years, it has been widely studied and used as a biomaterial, which refers to materials used for medical applications in organisms.

Wool:

Wool is the textile fiber obtained from sheep and other animals, including cashmere and mohair from goats, qiviut from muskoxen, from hide and fur clothing from bison, angora from rabbits, and other types of wool from camelids;[1] additionally, the Highland and the Mangalica breeds of cattle and swine, respectively, possess wooly coats.

Wool consists of protein together with a few percent lipids. In this regard it is chemically quite distinct from the more dominant textile, cotton, which is mainly cellulose.[1]

Manufacturing of Wool

Shearing

Sheep are generally shorn of their fleeces in spring but the time of shearing

differs in different parts of the world. Machine clippers remove the fleece faster

and closer than hand clippers. Superior wool variety comes from the sides and

shoulders where it grows longer, finer and softer is treated as good quality fleece.

Wool from the chest ,belly and shanks is treated as a second fleece.

Preparation

An average about 8 pounds of fleece is made from one sheep. Then the

fibers are packed in bags or bales. The raw wool or newly sheared fleece is

called Grease wool because it contains the natural oil of the sheep. When Greese

wool is washed, it loses from 20 to 80% of its original weight. The grease

known as yolk is widely used in the pharmaceutical industries for lanolin

compounds.

Sorting and grading

Skilled workers do wool sorting. Each grade is determined by type, length,

fineness, elasticity and strength. Separating of fibre by touch and sight.

Scouring

Washing of raw wool is an alkaline solution is known as scouring. The

wool is treated with warm water, soap, mild solution of soda ash or other alkali

to remove dirt in the fibres.

If the raw wool is not sufficiently clear of vegetable, substance after scouring

is put through the carbonizing bath. The fibres are then put through a dilute

solution of sulphuric or hydrochloric acid which destroys any vegetable. This

process is called as carbonizing and resultant wool is called ‘extract’.

To remove the Grease and dirt in raw wool it is put through a series of

naphtha balls followed by clear water to remove the naphtha. This is called

naphtalation. This process improves the dye uptake property of wool.

Garnetting

Recycled wool fibres are obtained by separately reducing the unused and

used fibrous mass by a picking and shredding process called garnetting.

Drying: Wool is not allowed to become absolutely dry usually about 12 to

16% of moisture is left in wool to condition it for subsequent handling.

Oiling: As wool is un manageable after scouring the fibre is usually treated

with various oils including animals, vegetable, mineral or a blend of these to

keep it from being becoming brittle o lubricate it for the spinning operation.

Dyeing: If the wool is to be dyed in raw stock it is dyed at this stage.

Some wool fabrics piece dyed, some are yarn or skin dyed and some are top

dyed.

Blending: Wool of different grades or pure wool fibres and other textile

fibers may be blended mixed together at this point. All the information should be

present on the labels.

Carding: The carding process introduces the classification of woolen yarns

and worsted yarns. It makes the fibre parallel and some amount of dirt is removed

due to straightening of fibres. Fibres are used for the worsted yarn are more

straightened than the wool yarns.

Gelling and combing: The carded wool which is to be made into worsted

yarn is put through gilling and combing operations. The geilling process removes

the shorter staple and straightens the fibre. This process removes short fibres

from 1 to 4 inch length places the long fibre as parallel as possible and further

cleans the fibre by removing any remaining loose impurities.

Drawing: Drawing is an advanced operation for worsted yarns which

doubles and redoubles slivers of wool fibres. The process draws, drafts, twists

and winds the stock making slivers more compact and thinning them into slubbers.

Roving: This is the final stage before spinning roving is actually a light

twisting operation to hold thin slubbers intact.

Spinning: In the spinning operation the wool roving is drawn out and twisted

into yarn. Woolen yarns are chiefly spun on the mule-Spinning machine are

worsted yarns are spun on any kind of spinning machine mule, ring, cap or flyer.

Properties of wool

Physical properties of wool

Strength: It is stronger than silk. When wet wool looses about 25% of its

strength. Longer the fibre the greeter will be the strength of yarn.

Resiliency: Wool is highly resilient and comes to its original shape when

hanged after wrinkled or created.

Stretch ability: Wool is highly elastic. It is about 10 to 30% stretched

when dry and 40 to 50% when wet upon receiving pressure upon drying it

readily regains its original dimensions.

Shrink ability: Wool is resistant shrinkage. However long exposure to

moisture may cause shrinkage.

Effect of friction: Friction will soften the wool fibre especially when wet

and thus is advantageous in maintaining smooth, soft texture of fabrics.

Crimps: Wool fibre is more or less wavy and has twists. This waviness is

termed as ‘crimp’. Finer the wool the more will be the crimps in it. Merino wool

has 30 crimps per inch while coarse wool has one or two.

Effect of moisture: Wool is the most hygroscopic in nature. It can absorb

up to 50% of its weight and carry up to 20% weight, without giving the feeling of

being wet. Upon drying it losses moisture slowly preventing rapid evaporation

thus avoiding chilling feel to the user. It absorbs perspiration after violent exercise

and guards the body against sudden change in temperature.

Heat conductivity: Wool fibre is a part is a poor conductor of heat and

therefore the fabrics made from the fibre are considered most suitable as winter

wear.

Felting: Wool fibres interlock and contract when exposed to heat, moisture,

and pressure. The scale like exterior of the fibres contributes to felting. The

fibres get softened in weak alkaline solutions due to expansion of scales at their

free edges, with friction and pressure they again interlock to form a felt. This

property is used in making felts for hats, shoes, floor-coverings and sound

proofing purposes.

Effect of heat: Low heat has no effect but strong heat weakens the fibre

and destroys the colour of the fibre.

Chemical properties

Action of acids: Dilute acids have little effect but either hot or concentrated

acids weaken or dissolve the wool fibres.

Action of alkalis: Alkalis tend to make while wool yellowish, strong

solutions of sodium carbonate when heated destroys the fibre sodium hydroxide

is highly injurious to the wool fibre. However borax and ammonia have no harmful

influence on wool.

Action of bleaching agents: Strong bleaching agents like hypochlorite

have harmful effects on wool., potassium permanganate, sodium peroxide and

hydrogen peroxide however can safely be used for bleaching and stain removal.

Effects of moth and mildew : Wool is easily damaged by moths that is

why during storage of woolen garments special case is needed. However mildews

do not effects garments.

Finishes given to wool: Felting, fulling, moth proofing, crabbing, decanting,

London shrinking, napping, singeing and steaming.

Wool blends: Wool polyester, wool acrylic, wool nylon, silk and wool.

Uses of wool

Firefighting

With flame retardancy up to 600 Centigrade, merino wool has long been the preferred material for firefighters’ uniforms. It doesn’t melt, shrink, or stick to skin when exposed to high temperatures, and has no toxic odours.

Carpets

Wool is a top choice for high-quality carpets. Dig down a layer and you’ll likely find it in the padding underneath. Yarn ends and substandard wool are not wasted. Instead they are put to good use manufacturing underlay.

Furniture:

Next time you take public transport note the seat upholstery. That’s yet another common usage of wool. Household upholstery as well, both stuffing and covers. Household use is as varied as it is ubiquitous. Blinds, curtains, lampshades, cushions, and wallpapers; the list goes on. Even those little felt pads you place under table and chair legs to protect the floor.

Bedding

We’ve used wool blankets in our homes for years. Now we’re taking a lead from our mates down under by producing duvets made from wool. The Aussies have been doing this for years. Except there they call them doonas, not duvets. As wool is a natural fire-retardant, it doesn’t need to be treated with chemicals to meet fire-safety standards.
Duvets filled with wool lead to a better night’s sleep compared to other fillings. That’s the conclusion drawn from research conducted by The University of Leeds and commissioned by The Wool Room. The temperature regulation qualities mean less overheating, hence a more restful night. In addition, the hypoallergenic properties make it eminently suitable for asthma and allergy sufferers.

Insulator

Wool in our walls keeps buildings both warm and quiet. Natural wool insulation is an environmentally-friendly acoustic and thermal option that is used across the world. All insulation has an R-value – a measure of its thermal resistance – and due to its ability to absorb and release moisture the performance of wool insulation exceeds its R-value rating. It’s a healthy option for installers too as they don’t need to wear any protective equipment when working with this natural product.

Fertilizer

The garden might be the last place you’d envisage using wool, but here again it has its place. Being absorbent and bio-degradable, wool makes a great mulch. Mulch pads made from wool provide an organic alternative to synthetic mulches. Taking it a step further, a project is under development in Italy whereby wool unsuitable for processing would be turned into fertilizer.

By-product

Wool is a low-waste product. Even the by-product, lanolin, has a myriad of uses from adhesive tape to auto lubrication as well as cosmetics and shampoos.

Other surprising uses

A mix of wool and seaweed is being used to reinforce bricks making them stronger and more environmentally-friendly. Left-over wool is used to produce wool-insulated packaging boxes. Additionally, wool has been successfully used to soak up major oil spills. You’ll even find it in pianos softening the impact of the hammers.

To fully cover the multitude of uses, we’d need to write a book. Wool has been used by man for centuries and is likely to be used for centuries to come.

There’s no doubt that we will keep developing new and innovative uses for this wonder fibre.

FLAX FIBER/ LINEN:

Flax is the most strongest among the natural cellulosic fibers. It is a bast fiber. Flax fiber is extracted from the skin of the stem of the flax plant. Flax is manufactured into linen yarn for thread or woven fabrics. So it is also called linen. It is also one of the oldest fibers, which was used more than 30,000 years before. Linen cloth made from flax was used to wrap the mummies in the early Egyptian tombs.

Fig: Flax fiber

PHYSICAL PROPERTIES OF LINEN FIBRES:

- Strength: An important property of linen is its strength. Linen is a durable fiber, as is two-three times as strong as cotton. It is second in strength to silk. It gives the same comfort like Cotton fiber.

- Elasticity: Elasticity is the extent to which a fiber can be elongated or stretched and then returned to its normal condition and size. Linen is the least elastic natural fabric.

- Resilience: Resilience refers to the extent to which a fabric can be deformed by crushing or compressing it, and finally returning it to its original condition. Linen is quite stiff and wrinkles easily.

- Absorbency: Absorbency refers to the extent to which moisture can penetrate into a fiber. Another linen property is that the fiber absorbs moisture and dries more quickly. It is excellent for manufacturing towels and handkerchiefs.

- Heat Conductivity: Heat conductivity refers to the extent to which heat can be conveyed through a fiber. Heat conductivity of linen is five times as high as that of wool and 19 times as that of silk. It is most suitable for use in summers, as the fiber allows the heat to escape, leaving a cool effect. Studies have shown that with linen clothes perspiration is 1.5 times less than when dressed in cotton clothes. It is twice less than when dressed in viscose clothes. Meanwhile in cold seasons linen is an ideal warmth-keeper.

- Comfortable: Linen is a comfortable fabric. Being natural vegetable fibers it has huge amount of Air Porosity hole, which make the linen clothes very comfortable to wear.

- Crisp: The linen fabric has a crisp feel with a distinctive outlook and feel. Linen possesses a natural crispness when ironed damp. Hence it does not require starching, and has a natural luster.

- Lightweight/Heavyweight: You will find any kind of linen fabric or linen fibers in any weight in the market.

- Good Abrasion Resistant: As the linen fiber is good in strength, it also has good abrasion resistance.

- Resistant to Allergy: No kind of allergic reactions are caused using linen and hence it is helpful in treating a number of allergic disorders.

- Anti inflammatory property: Linen is helpful in dealing with inflammatory conditions, reducing fever, regulating air ventilation, in some neurological ailments.

- No static electricity: Another property of linen is that it does not accumulate static electricity. Since line is made of flax, even a small addition of flax fibers to a cloth is sufficient to reduce or eliminate the static electricity effect.

- Lusture: It is brighter than cotton fiber and it is slightly silky.

- Hand Washable & Dry Cleanable: You can not only wash the clothes linen but also clean the lien clothes by drying. So, making linen clothes by using the linen fiber is a wise decision for the Textile Industry owner.

- Tailors Well: One textile weavers or textile knitter can easily make the Linen fabric by using the flexible linen fiber and the tailors of the Garment Shop, even can easily make Dress and suits by using the Linen fabrics.

- Dyes & Prints well: Along with the optimum efficiency in Dyeing, one can easily print the Linen cloth except for any kind of problems like print paste saturation, discolored surface etc.

- Lightweight To Heavyweight: Any kind of linen fabric or linen fibers are available on the market which can be achieved in any weight as per the Textile buyers’ requirement.

- No Static & Pilling problems: If any fabric produces the static electricity during wear, then nothing can be worst than that. People like to wear the fabric that is flexible and comfortable to wear. Linen is the perfect fabric in this regard which has no static electricity and pilling problems.

### Chemical properties of Linen

-       Effects of alkalis: Resistant to alkalis and comparatively unaffected by normal laundering. The resistance is because of the lack of attraction between the flax polymers and alkalis.

-       Effect of Acids: Weakened and destroyed by acids. Acids hydrolyze the flax polymer at the glycosidic oxygen atom which connects the two glucose units to form the cellobiose unit. Mineral acids being stronger than organic acids will hydrolyse the flax polymer more quickly.

-       Effect of Bleaches: The most common bleaches used on linen textile materials are sodium hypochlorite and sodium perborate. They are: oxidizing bleaches and bleach because of the oxygen liberated from them.

-       Effect of Sunlight and weather: The ultra-violet rays of sunlight provide photo chemical energy whilst the infra-red rays provide heat energy essential to degrade the linen polymers in the pressure of atmospheric oxygen, moisture and air pollutants. The breakdown of polymers takes place through diverse hydrolysis reactions. The beginning degradation is noticed as a slight fibre discoloration. Fading of colored flax textile is partially because the breakdown of the dye molecules in the fiber’s polymer system.

-       Color Fastness: Flax is easy to dye and print. The classes of dye which may be used to color flax are azoic, direct, reactive, sulphur and vat dyes. The polar polymer system easily attracts any polar dye molecules into the polar system. Therefore, dye molecules which can be dispersed in water will be absorbed by the polymer system of flax.

However, the dye molecules can enter solely the amorphous regions of the polymer system of flax. The small inter polymer spaces in the crystalline regions of the polymer system prohibit the entry of the crystalline molecules.

-       Mildew: Flax is damaged by fungi. Heat and dampness support the growth of mildew. The fungi produce a chemical compound which has the power of changing cellulose to glucose. The fungi feed on the molecules of sugar: Flax treated with acrylo nitrite is resistant to mildew.

-       Insects: Moths and beetles do not change flax. Silver fish will eat flax cellulose especially if heavily starched.

USES OF LINEN FIBRE:

Linen is an elegant and durable fabric. Linen is a fiber that is taken from the flax plant. In addition to being a strong fabric, it is also smooth. Linen does wrinkle easily, but the wrinkles are released easily if you iron them. The fact that linen is lint free and has a fine luster makes it popular for use in clothing and house wares. It is recommended for clothing in warm climates.

Flax is two to three times stronger than cotton fiber, but less elastic. The best grades are used to make linen fabrics such as damasks, sheeting and lace. Coarser grades are used for the manufacturing of rope and twine, and historically for canvas and webbing equipment. Flax fiber is also used as a raw material in the high-quality paper industry for the use of printed banknotes and rolling paper for tea bags and cigarette paper manufacture. It is also hypo-allergenic and so an excellent choice of fiber for those with allergies

## Tablecloths

A popular use of linen is in tablecloths. Linen is used by many people as it is more durable than cotton. Also, unlike most other fabrics, it actually becomes more durable when it is wet. As there are often liquid spills at the dinner table, this makes it less likely to be damaged.

## Napkins

Napkins are often made of linen for similar reasons as tablecloths. They contribute nicely to a formal table and will not be damaged by spills and wetness, which is important as they are often used to clean up liquids that spill at the table. In addition, they do not pill as much as other fabrics do.

## Clothing

Linen is often used in clothing, particularly in warm climates. It tends to be a cooling fabric in hot weather. As it is woven and lightweight, it allows the air to pass through it, which gives the cooling effect. Linen is often seen in shirts, pants and dresses. As it wrinkles easily, you will have to iron it more often. If you sweat in it though, it will not be damaged.

## Decorating

Use linen to re-purpose and decorate your home. This is a particularly good idea if you have old linens that you would like to use. One way to recycle them is to cut them up and use them as coasters for drinks. Another idea is to use old pillowcases and make them into tablecloths. These ideas are both budget and environmentally friendly.

BANANA FIBRE

Banana fiber is a natural fiber with high strength, which can be blended easily with cotton fiber or other synthetic fibers to produce blended fabric & textiles. Banana Fiber also finds use in high-quality security/ currency paper, packing cloth for agriculture produce, ships towing ropes, wet drilling cables etc.

Characteristics of Banana Fibers: 
Banana fiber has its own physical and chemical characteristics and many other properties that make it a fine quality fiber.

Appearance of banana fiber is similar to that of bamboo fiber and ramie fiber, but its fineness and spin ability is better than the two.

- The chemical composition of banana fiber is cellulose, hemi cellulose, and lignin.

- It is highly strong fiber.

- It has smaller elongation.

- It has somewhat shiny appearance depending upon the extraction & spinning process.

- It is light weight.

- It has strong moisture absorption quality. It absorbs as well as releases moisture very fast.

- It is bio- degradable and has no negative effect on environment and thus can be categorized as eco-friendly fiber.

- Its average fineness is 2400Nm.

- It can be spun through almost all the methods of spinning including ring spinning, open-end spinning, bast fiber spinning, and semi-worsted spinning among others.

Banana Fiber Extraction Processing, Yarn Spinning & Weaving:

Fig: Extraction of Banana Fiber from bark of Banana plant.

The extraction of the natural fiber from the plant required certain care to avoid damage. In the present experiments, initially the banana plant sections were cut from the main stem of the plant and then rolled lightly to remove the excess moisture.

Impurities in the rolled fibers such as pigments, broken fibers, coating of cellulose etc. were removed manually by means of comb, and then the fibers were cleaned and dried. This mechanical and manual extraction of banana fibers was tedious, time consuming, and caused damage to the fiber. Consequently, this type of technique cannot be recommended for industrial application.

A special machine was designed and developed for the extraction of banana fibers in a mechanically automated manner. It consisted mainly of two horizontal beams whereby a carriage with an attached and specially designed comb, could move back and forth. The fiber extraction using this technique could be performed simply by placing a cleaned part of the banana stem on the fixed platform of the machine, and clamped at the ends by jaws. This eliminated relative movement of the stem and avoided premature breakage of the fibers. This was followed by cleaning and drying of the fibers in a chamber at 200 C for three hours. These fibers were then labeled and ready for lamination process. 

After fiber is collected, the process goes to yarn spinning. The researcher investigated the traditional process, which use the filament yarns in weaving banana fabric. The finding showed that the convention process was very time-consuming, thus not appropriate for today’s use. Therefore, this research explored open-ended spinning process for yarn development. The fiber was cut in to 3-centimeter length for spinning process.

Applications of Banana Fiber:

Fig: Uses of Banana fibers.

In the recent past, banana fiber had a very limited application and was primarily used for making items like ropes, mats, and some other composite materials. With the increasing environmental awareness and growing importance of eco-friendly fabrics, banana fiber has also been recognized for all its good qualities and now its application is increasing in other fields too such as apparel garments and home furnishings. However, in Japan, it is being used for making traditional dresses like kimono, and kamishimo since the Edo period (1600-1868). Due to its being lightweight and comfortable to wear, it is still preferred by people there as summer wear. Banana fiber is also used to make fine cushion covers, Necties, bags, table cloths, curtains etc. Rugs made from banana silk yarn fibers are also very popular world over.

JUTE:

Jute is a bast fiber used for sacking, burlap, and twine as a backing material for tufted carpets. It is a long, soft, shiny fiber that can be spun into coarse, strong threads. It is one of the cheapest natural fibers, and is second only to cotton in amount produced and variety of uses. Jute fibers are composed primarily of the plant materials cellulose, lignin, and pectin. Both the fiber and the plant from which it comes are commonly called jute. It belongs to the genus Corchorus in the basswood family, Tiliaceae.

Fig: Jute fibre

## Production

Jute stems being retted in water to separate the fibers

The jute fiber comes from the stem and ribbon (outer skin) of the jute plant. The fibers are first extracted by retting. The retting process consists of bundling jute stems together and immersing them in slow running water. There are two types of retting: stem and ribbon. After the retting process, stripping begins; women and children usually do this job. In the stripping process, non-fibrous matter is scraped off, then the workers dig in and grab the fibers from within the jute stem.[6]

Jute is a rain-fed crop with little need for fertilizer or pesticides, in contrast to cotton's heavy requirements. Production is concentrated mostly in Bangladesh, as well as India's states of Assam, Bihar, and West Bengal.[7] India is the world's largest producer of jute,[8] but imported approximately 162,000 tones[9] of raw fiber and 175,000 tones[10] of jute products in 2011. India, Pakistan, and China import significant quantities of jute fiber and products from Bangladesh, as do the United Kingdom, Japan, United States, France, Spain, Ivory Coast, Germany and Brazil.

Properties of Jute Fiber:

- Jute fibre is 100% bio-degradable and recyclable and thus environmentally friendly.

- Jute is a natural fibre with golden and silky shine and hence called The Golden Fibre.

- Jute is the cheapest vegetable fibre procured from the bast or skin of the plant's stem.

- It is the second most important vegetable fibre after cotton, in terms of usage, global consumption, production, and availability.

- It has high tensile strength, low extensibility, and ensures better breathability of fabrics. Therefore, jute is very suitable in agricultural commodity bulk packaging.

Length

The reeds of Jute fibre vary from 3 to 14 feet long, depending on the grade, and they show taper from root to end. Thick reeds contain coarse fibre and thin reeds contain finer fibre. It constitutes with ultimate fibres of average length of 2.5mm.

Fineness

It is a coarse fibre. Its diameter varies from 6 to 20 microns.

Strength

Fibers are not so strong when compared with some other bast fibres but have good tensile strength. Fibres are naturally hard and brittle and break off with abrasion. Resistance to mechanical wear is low and not durable especially on exposure in moisture reduces its strength. Its extension at break is 2%.

Color

The best quality fibres are pale white or silvery grey, common qualities are brownish and greenish are inferior, roots are usually darker without any luster. Better quality fibres shows matt and pitted surface with very poor strength.

Luster

Better quality fibres have fairly high luster but inferior quality fibres shows matt and pitted surface with very poor strength.

Roots

Base portion of the Jute stems is more rigid and has a stronger supporting bark than the rest of the stem. This is due to longer exposure of this part to the action of the sunlight and water. During grade shorting, the root portion are removed by cutting and baled separately known as bale cutting.

Cleanliness

Cleanliness of fibre is an essential factor for high grade. Adhering portions of bark, specks sticks etc. are undesirable which affects grading according to their degree of presence.

Effect of chemicals

- Water: Jute is a hygroscopic fibre i.e. it takes in or gives out moisture to its surrounding atmosphere. Under standard testing atmosphere, moisture content value is 12.8% and moisture regain value of this fibre is 14.6%.

- Acid: This fibre is damaged by the action of strong acid hence wet processing on Jute fibre is not done in acid medium.

- Alkali: It is safe in alkali medium; hence wet treatment is done on alkali medium.

The best source of Jute in the world is the Bengal Delta Plain, which is occupied by Bangladesh and India.

Uses of Jute Fiber
Jute is the second most important vegetable fibre after cotton; not only for cultivation, but also for various uses.

- Jute is used chiefly to make cloth for wrapping bales of raw cotton, and to make sacks and coarse cloth.

- The fibres are also woven into curtains, chair coverings, carpets, area rugs, hessian cloth, and backing for linoleum.

- While jute is being replaced by synthetic materials in many of these uses, some uses take advantage of jute's biodegradable nature, where synthetics would be unsuitable.

- Jute butts, the coarse ends of the plants, are used to make inexpensive cloth.

- Traditionally jute was used in traditional textile machineries as textile fibres having cellulose (vegetable fibre content) and lignin (wood fibre content). But, the major breakthrough came when the automobile, pulp and paper, and the furniture and bedding industries started to use jute and its allied fibres with their non-woven and composite technology to manufacture nonwovens, technical textiles, and composites.

- Jute can be used to create a number of fabrics such as Hessian cloth, sacking, scrim, carpet backing cloth (CBC), and canvas.

- Hessian, lighter than sacking, is used for bags, wrappers, wall-coverings, upholstery, and home furnishings.

- Sacking, a fabric made of heavy jute fibres, has its use in the name.

- Diversified jute products are becoming more and more valuable to the consumer today. Among these are espadrilles, floor coverings, home textiles, high performance technical textiles, Geo textiles, composites, and more.

- Jute is also used in the making of ghillie suits which are used as camouflage and resemble grasses or brush

Thus, jute is the most environment-friendly fibre starting from the seed to expired fibre, as the expired fibres can be recycled more than once. 
Another diversified jute product is Geo textiles, which made this agricultural commodity more popular in the agricultural sector. It is a lightly woven fabric made from natural fibres that is used for soil erosion control, seed protection, weed control, and many other agricultural and landscaping uses. The Geo textiles can be used more than a year and the bio-degradable jute Geo textile left to rot on the ground keeps the ground cool and is able to make the land more fertile.

PINE APPLE:

Many health conscious people love to have Pineapple as their favorite dessert. It’s because of many health benefits of the delicious fruit. It protects from a simple flu as well as fights off free radicals that cause cancer. It cleans the internal system to keep our body healthy through fibers that help in proper digestion. That’s not all, it’s not the only kind of fiber that a pineapple carries. Pineapple leaves are used to obtain Piña, a textile fiber that is used to make fabrics. As such, we are able not only to keep our internal system clean but also to achieve an outer elegant appearance. Piña is a pineapple fiber made from the leaves of a pineapple plant and is commonly used in the Philippines. It is sometimes combined with silk or polyester to create a textile fabric. Piña’s name comes from the Spanish word piña which literally means pineapple

Production of pineapple fiber

Since piña is from a leaf, the leaf is cut first from the plant. Then the fiber is pulled or split away from the leaf. Most leaf fibers are long and somewhat stiff. Each strand of the Piña fiber is hand scraped and is knotted one by one to form a continuous filament to be hand-woven and then made into a Piña cloth. Researchers have developed some easy tools to extract fiber from pineapple leaves.

Fiber from Pineapple leaves for long has been used by Philippine handicraft artisans to produce cloth. Pineapple fibre is considered to be more delicate in texture than any other vegetal fibre. A kilo of leaves may provide up to 15-18 pieces of white, creamy and lustrous as silk fibre about 60 cm long and it easily retains dyes.

It is a painstaking process and involves up to 30 people from the beginning to the end of the process. Fibres of the leaf are scrapped by means of a broken plate or coconut shell and a fast scraper can extract fibre from over 500 leaves per day after which the fibres are washed and dried in the open air.

After which they are waxed to remove the entanglements and then the fibres are knotted and bind into yarns for the next process of weaving it in to fabric. Pineapple fabrics are mainly used for creating Barong Tagalog and other formal wear. It is also used for other products where a lightweight, but stiff and sheer fabric is needed.

It is sometimes combined with silk or polyester to create a textile fabric.

Properties of PALF or pineapple leaf fibre:

- Optical microscope - PALF is multi cellulose fibre like other vegetable fibre. Cells in the fibre have an avg. diameter of about 10 micron and mean length 4.5 mm.

- Electronic microscope - PALF has a scaly cellular structure with vegetable matter intact. In raw fibre, lumen is present in cross section , hollow structure represent that PALF will have high insulation power and high absorbency.

- Physical characteristic - ( Ultimate cells )

- Thermal property - Thermal conductivity of PALF is found to be low at 0.0273 watts/m2/k which suggest that these fibres could be used as good thermal insulators.

Chemical property of PALF:

- Effect of Alkali - When the PALF is treated with 18% NaoH it enhances the breaking elongation and it also result in length shrinkage.

- Effect of H2O2 - Hydrogen peroxide improve its fineness by 5 to 6 %, but reduces tensile strength by 40 to 45 % .

- Dyeing property - PALF has higher dye absorption tendency as compared to cotton due to its higher moisture regain.

Uses of pineapple fibers

Pineapple fibers, primarily used in hand weaving are divided into two groups- the linuan or fine fibers and bastos or coarse fibers. Red Spanish or native variety of piña is mainly used for hand weaving to make valuable items such as traditional Barong Tagalog, wedding attire for men, and blouses for women , kimonos, panuelos, handkerchiefs, table linen, mats, fans, gowns, and other clothing. The smooth Cayenne or Formosa varieties are primarily used in development of Philippine Tropical Fabrics.

A major use for piña fabric is in the creation of the Barong Tagalog and other formal wear that is common in the Philippines. It is also used for other table linens, bags, mats and other clothing items, or anytime that a lightweight, but stiff and sheer fabric is needed.

The pina fabric is decorated by a traditional style of hand embroidery called calado. An embroidered piña garment is known as piña calado. These hand woven fabrics are dyed with vegetable dyes obtained from leaves and bark of various trees. Pina fiber is often blended with cotton, abaca, and silk to make amazing light and breezy fabrics. When woven with silk, it is known as pina seda or pina-silk. Pina jusi is a blend of abaca or silk for strength and sheerness and is less expensive than 100% pina.

OTHER NATURAL FIBRES

KAPOK FIBRE 
KAPOK fibre is one of the natural cellulose fibre which grown on kapok plant. This fibre is also known as silk cotton because its natural luster is similar to that of pure silk. kapok is similar to cotton but it can be easily distinguished, when it tested under microscope. short length and smooth surface of fibre, causes poor interfiber friction so that it can be easily processed on modern spinning machine.

Fig: Kapok fibre

Properties of kapok fibre:

- Average linear density - 0.064 tex

- Average diameter - 2.5 micrometer

- Average length - 20 mm

- Fineness - 0.4 - 0.6 denier

- Tenacity - 1.4 to 1.74 gm/den.

- Elongation at break -1.8 to 4.23

- Absorbency - kapok fibre has high lumen percentage, because of this it has excellent oil absorbency and retention capacity.

- Lightweight - kapok fibre is 8 time lighter than cotton by volume

- Effect of acid - kapok fibre shows good resistance to acid and it not affected by acid.

- Effect of alkali - kapok fibre is not affected by alkali, that shows good resistance to alkali.

End uses of kapok fibre-

- Mattress

- Clothing

- Technical textile

- Insulating material

- Medical textile

- Cushions

- Upholstery furniture

- Life jackets

SISALFIBRE 
‘SISAL’ is the most widely used natural fibre and its cultivation is comparatively easy. It is obtained from sisal plant. Scientific name of sisal fibre is ‘Agava sisalana’. Sisal plant consist of a rosette of sword-shaped leaves about 1.5 to 2.00 meters tall. The sisal fibre has a 7 to 10 years life span and typically produces 200-250 commercially usable leaves. Each leaf contain an average of about 1000 fibre. The fibre are account only for 4% of plant by weight. Sisal fibre are made from the large spear shaped tropical leaves of Agava sisalana plant. Sisal fibre are extracted by a process known as decortication. Sisal fibre is fully biodegradable and it is highly renewable resource of energy. Sisal fibre is exceptionally durable and low maintenance with minimum wear and tear. fibre is too tough for textile and fabrics. It is not suitable for smooth wall finish and also not recommended for wet areas. Sisal fibre has an average length of 0.6 to 1.2 meter, and it is creamy white to yellowish in colour.

Fig: Sisal fibre

Properties of sisal fibre:

- Sisal is exceptionally durable and recyclable.

- It is antistatic, does not dust particle and does not absorb moisture or water easily.

- Fine fibre ( from outer leaf skin ) takes dyes easily, offers the largest range of dyed colour.

- It has good sound and impact absorbing property.

- Its leaves can be treated with natural borax for fire resistance property.

- Sisal fibre is creamy white in colour.

- Avg.fibre length 80 to 120 cm and 0.2 to 0.4 mm in diameter

- Coarse and inflexible.

End uses (Application) of Sisal fibre:

- Paper industry (lower grade fibre)

- Ropes (medium grade fibre)

- Carpets (higher grade fibre)

- Filters

- Geo textile

- Mattresses

- Handicrafts

- Wire rope cover

- Woven floor covering etc.

BAMBOOFIBRE 
‘BAMBOO’ fibre is cellulose fibre extracted from natural growth of bamboo, is the fifth natural fibre following the cotton, linen, wool and silk. Bamboo is fastest growing woody plant on this planet. It grows one third fastest than fastest growing tree. Sometime growth of bamboo is approximately three feet over day. Bamboo fibre comes from nature, and completely returns to nature in end, therefore bamboo fibre is praised as ‘Natural, green and eco friendly new type of textile material of 21st century’. Bamboo is biodegradable textile material. As natural cellulose fibre, it can be 100% biodegradable in soil by microorganism and sunlight. Its decomposition process doesn’t cause any pollution environment. Bamboo products are further characterized by its good hydrophilic nature, excellent permeability, soft feel, excellent dyeing behaviour and its antibacterial property.

Fig: Bamboo fiber

Properties of bamboo fibre:

- Bamboo fibre has good durability, luster, stability, moderate tenacity and good spin ability.

- It is naturally antibacterial, UV protective, biodegradable, breathable cool, strong flexible, soft and it has better shiny appearance.

- Bamboo fibres are further characterized by its good hydrophobic nature, good permeability, soft feel, excellent dyeing behavior and its antimicrobial property.

- Bamboo fibres absorb and evaporate moisture quickly.

- It is more breathable, so it give better comfort to wearer.

- Bamboo fibre has various micro gaps and micro holes leading to much better moisture absorption and ventilation.

- Bamboo fibre can be softer than silk fibre when spun into yarn.

USES

● Apparel textile :

- Sweaters

- Bath suits

- Mats

- Blankets

- Towels

- Underwear

- Socks

● Medical textile :

- Sanitary napkins

- Masks

- Mattress

- Food packaging bags

- Bandage

- Gowns

- Surgical cloth

● Home textile:

- Curtains

- Wall paper

- Sofa covers

- Table cloth

- Bed sheets