Desizing

Desizing is the process of removal of size material applied on warp threads of a fabric to facilitate the process of weaving. Size forms a stiff, hard and smooth coating on warp yarns to enable them to withstand the cyclic tensions during weaving and reduce breakage.

Removal of impurities

In general the impurities from textile substrates can be removed by following processes:

Solubilization. Emulsification. Chemical breakdown by; Hydrolysis. Oxidation.

In case the size is not soluble, it is removed by either hydrolysis or oxidation. Hydrolysis or oxidation results in lowering of molecular weight of starch, which results in improved solubility of degraded starch. Following parameters play an important part in determining the efficiency of any desizing or other pretreatment process:

Important parameters

Temperature. pH. Time. Circulation. M:L ratio.

HYDROLYTIC DESIZING :

Mechanism of hydrolytic desizing :

Starch consists of both amylose and branched amylopectin which are poly -α-glucopyranose. The glucose units in both are linked at 1-4 positions. In case of amylopectin, certain linkages also occur at 1-6 positions (~4%). When the 1-4 linkage is attacked and broken by hydrolysis, the desizing is called hydrolytic desizing. Initial starch degradation product is insoluble dextrin, which on further hydrolysis is converted to soluble dextrin and finally glucose.

HYDROLYTIC DESIZING METHODS :

ROT STEEPING-

- Steeping in water at 30-400C, starch swells - Swollen starch is attacked by enzymes secreted by microorganisms in environment - Hydrolyzed starch is removed by normal washing - Low capital investment - Slow, low reproducibility, risk of cellulose being attacked

Rot steeping has become obsolete because of poor process control and slowness of the process.

ACID DESIZING:

The 1-4 linkage can be broken by acid hydrolysis also. Mineral acids are used.

- H 2SO 4/HCl- (5-10 gpl) is needed at 400C for 3-4 hours. - Above 400C & 10 gpl acid concentration, degradation of cotton cellulose itself may occur. - The fabric is padded with acid solution and stored (batched). - Action of acid will result in gradual degradation of starch. But not all starch is degraded to the extent where it all becomes water soluble. - Hence the action of acid will result in fabric having a range of starch molecular weights. Some with high water solubility, some with medium and some with poor or no solubility. - Hence desizing should always be followed with hot water washing to remove maximum amount of starch.

Precaution - Local drying during storage should not be allowed to take place at any cost. It may result in high concentrations of acid at localized places which can cause cellulose degradation.

ENZYMATIC DESIZING:

In Greek enzyme means - in yeast

The term was coined in 1876 by German biochemist Willey Kuhne.

Enzymes are:

- Organic biocatalyst, highly specific in reaction catalyzed and choice of reactants/substrate and hence safe to the substrate - Physically---- colloidal in nature - High molecular weight proteins (3-D) - Work under specific conditions of temperature and pH hence better process control is needed - Lose activity gradually with time - Generally act under mild conditions - Have to be cultivated and nurtured like crops (from fungi) - Genetic engineering allows enzymes to be designed for specific processes

Enzyme Sources For Desizing :

Vegetable, bacterial, Animal

(Diastase, Rapidase, Amylase etc.)

Malt Amylase has two components:

α & β - Amylase (Ratio 1:5 to 1:6)

α- Amylase attacks the chain at random

β -Amylase attacks the chain end & produces maltose

Since enzymes act optimally at specific conditions of temperature and pH, it is important to maintain narrow range of conditions for best results.

The optimum process conditions for various enzymes vary. The table given below compares the best process conditions for these enzymes.

Since grey cotton has poor absorbency, surfactants can be used to improve the wetting of fabric and dispersion of hydrophobic impurities. In general, anionic surfactants inhibit enzyme action. Non-ionic surfactants are generally preferred.

Although traditionally enzymes are used under mild process conditions, genetic engineering has allowed development of robust enzymes which can be used at higher temperatures to increase the rate of desizing.

High temperature enzymatic desizing :

Novozymes, an enzyme producing major, introduced an alkaline amylase with a broad activity spectrum, capable of application over the pH range 5-10 and from 20-85°C. This has enabled combined desizing and bioscouring to achieve commercial acceptance in a number of textile mills. They have also developed enzymes for use in high temperature. The details are given below:

Aquazym® PS ( Novozymes)

A heat-stable alpha-amylase used in high-temperature continuous desizing processes (Pad Steam).

Aquazym® SD ( Novozymes)

It is a flexible amylase that works well at broader pH and temperature ranges than conventional amylases

Enzyme product; Temp. (°C); pH; Continuous; Pad-roll; Jet, jig, winch. Aquazym® PS; 85-115; 5.5-6.5; +++; NR; +/-. Aquazym® SD; 20-85; 5.5-6.5; +++; NR; +/-.

Sodium & Potassium chloride (0.2-1%) improve the activity of pancreatic enzyme.. Ca++ improves the thermal stability of malt amylase. However, sequestering agents and heavy metal ions like copper, iron etc. inhibit their activity..

Oxidative desizing

In oxidative desizing, the size is removed by oxidative degradation. It is particularly useful when the size is based either on a synthetic polymer like PVA (poly vinyl alcohol) or is a mixture of synthetic and natural polymers. Hydrolytic desizing is successful in case of natural starch but is does not remove sizes based on synthetic polymers.

Following oxidative agents are used in oxidative desizing:

Hydrogen peroxide (H2O2). Sodium bromite (NaBrO2). Sodium and potassium persulphate (Na 2S2O8, K 2S2O8). Sodium chlorite (NaClO2). Peroxy monosulphuric acid (H2SO5).

With sodium chlorite, the desizing is carried out under alkaline conditions.

Sodium bromite is a powerful oxidant for starch. It breaks glucose ring by breaking C2-C3 link and produces a dialdehyde. This dialdehyde dissolves in alkaline solution hence desizing is followed by an alkaline wash. It acts best at pH 10. It works at room temperature for short durations and is highly efficient.