J-Box:

After application of liquor by padding, the required time for chemicals to act on impurities is provided in a J-box or batching tray or steamer. J-Box is one of the popular machines generally used in scouring of cotton fabrics. J-box is essentially a J-letter shaped stainless steel chute with large fabrics holding capacity. The fabric is fed from one end & taken out of the other (First in first out) in contrast to a keir where it is first in last out. The J-box has a polished inner side and it is insulated to minimise heat losses.

The fabric after saturation with liquor (from a saturator located just in front of J-box) is fed from the top and taken out from the lower end. Depending on fabric speed (150-300 m/min) and the capacity (10,000 m) a residence time of 60-90 min may be provided. Fabric may be heated at the entry to the J-box and may retain the temperature due to insulation inside the chamber. M:L ratio 1:1.

After coming out from the J-box, the fabric is sent to a washer.

In continuous processing, it makes sense to combine various processes to save time, water, energy manpower etc. Combining desizing and scouring in case of cotton is possible by using oxidative desizing agents which can work in alkaline medium. Similarly, scoring and bleaching can be carried out in two continuous stages in one operation. This is shown in the schematic shown below.