## Slide 1
SUBJECT : (19CDU17) TEXTILE FINISHING TECHNOLOGY
CLASS : III BSc –CDF

## Slide 2
Onlineclass(Googlemeet) Prepared by : V.Deepa Class: III.B.Sc CDF 10/08/2021
Soil or stain Repellency :
Soil release fnishes reduce the degree o soiling o theabric by repelling the soil or by preventing ormation oa bond between soil and abric. They improve a abric’s perormance in resisting soil,releasing soil and retaining whiteness by resisting redeposition o soil rom the wash water. The abric cannot be made soil resistant but a type ofnish is given to the abric so that during washing, theaccumulated soil on the abric can be easily removedrom the abric This type o fnish is !nown as soil repellent, stainresistant or anti soil or anti stain fnishes.
UNIT – 3
CHEMICAL FINISHES:
Functional finishes – methods and applications –wrinkle free finishes, water repellant finish, flame retardant finish, antistatic finish, and soil release finish, silicone finish, anti bacterial finish, and phase change finishes, rot and mildew proof finish, Special purpose finishes – methods and applications –denim finish – stonewash and enzyme wash; fragrance finish, UV protection finish,

## Slide 3
Onlineclass(Googlemeet) Prepared by : V.Deepa Class: III.B.Sc CDF 10/08/2021
FUNCTIONAL FINISH:
These are wet processes used to produce special effects on fabrics or to improve specific properties. Many of these effects are required to increase the customer appeal of products or to augment fabric properties for particular end-uses, such as outdoor wear or protective clothing.
Absorbency finish : Although the cellulose fibers like cotton, linen and rayon have good absorbency, sometimes it is desired that they should be more absorbent.
Appropriate application of ammonium compounds modifies the cellulose to become more absorbent, providing greater comfort and usefulness for such uses as undergarments and towels.

## Slide 4
Onlineclass(Googlemeet) Prepared by : V.Deepa Class: III.B.Sc CDF 10/08/2021
Wrinkle resistant finish : These finishes are also sometimes referred to as 'crease-resistant' or 'Wash and wear' finishes. DMDHEU namely Dimethyl Dihydroxy Ethylene Urea is used to impart wrinkle resistant finish on the textiles.
The purpose of this finish is to prevent deformation of the fabric by undesirable and unintentionally introduced folds and rumples.
Some finishes are more wrinkle-resistant than others, but fabrics treated with any of these finishes tend to smooth out when properly hung after wearing.

## Slide 5
Onlineclass(Googlemeet) Prepared by : V.Deepa Class: III.B.Sc CDF 10/08/2021
Flame retardant finish : A wide variety of flame retardant chemical finishes have been developed for application to fibers and fabrics. Carbonate and ammonium salts are used for flame retardant finish.
Antibacterial finish : Chemical antiseptic finishes using Chitosan, impart a self-sterilizing quality to a fabric. The appearance and the feel of the fabric does not change and no chemical odour remains. Dry cleaning does not impair the finish.
Prevention of mildew : Cellulose fibers are particularly susceptible to mildew. Silk and wool are also susceptible, but to a lesser extent. Such untreated fabrics will become stained, malodorous and eventually deteriorated by the fungus if allowed to remain in a moist condition for a period of time.

## Slide 6
Onlineclass(Googlemeet) Prepared by : V.Deepa Class: III.B.Sc CDF 10/08/2021
Shower curtains or other fabrics may be mildew proofed at home by soaking the material in soapy water, then, without rinsing, dipping it into a solution of boric acid and carbolic acid, which prevents rapid growth of the mildew fungus.
The most effective mildew proofing agent is 0.05 per cent solution of phenyl mercuric acetate in water.
Water repellent finish : The fibres in the fabrics become covered with a film of synthetic resin. This repels and delays adsorption and penetration of water through the fabric. This finish allow air to permeate the fabric, and its comfort is largely retained in contrast with the water proof finishes.

## Slide 7
Onlineclass(Googlemeet) Prepared by : V.Deepa Class: III.B.Sc CDF 10/08/2021
Waterproof finish : For a fabric to be truly waterproof, it must be completely sealed with a substance that is insoluble in water. Modern waterproofing materials include the vinyl resins, which do not oxidize and crack as readily as rubber.
Wash-n-wear:
When wash‘n’ wear finish is applied on cotton, itdoes not wrinkle too much and becomes easy to maintain.
If dried and handled properly, wash ‘n’ wearfabrics can be worn without ironing or with alittle ironing.

## Slide 8
Onlineclass(Googlemeet) Prepared by : V.Deepa Class: III.B.Sc CDF 10/08/2021
https://docs.google.com/forms/d/e/1FAIpQLSepkyZrcx0rqL0XG7jOoEP4DJ4lbDSulzU7Pvn5Mi3UhQqRMQ/viewform?usp=sf_link
MCQ