UNIT - 5

Current Trends in Textile finishing: Definition -Application of Nano technology in textiles- Water repellence, U.V Protective finish, Self cleaning fabrics, Antistatic finish, Wrinkle free treatment.

Microencapsulation – Definition, Objectives, Structure & Characteristic of Micro encapsules, Application of Micro encapsules in Flame retardant, Medical application, Anti microbial and Fragrance finish.

Plasma technology – Definition, Application of plasma technology in Desizing, Water / Soil repellency finishes. Merit and Demerits of Plasma Technology Aqua finish – Definition.

MICRO ENCAPSULES:

Objectives of Encapsulation

Encapsulation of active ingredients for a wide range of industries is carried out for one or more of the following purposes:

- Rendering liquids into powders to prevent clumping and improve mixing.

- Protecting active ingredients from oxidation, heat, acidity, alkalinity, moisture or evaporation.

- Preventing ingredients from interacting with other compounds in the system, this may result in degradation or polymerization.

- Masking the taste of unpleasant flavors or odors.

- Improving the handling of an ingredient before processing.

- Release active chemicals in a controlled or targeted fashion.

- Protecting workers or end users from exposure to hazardous substances.

Microcapsules Structure

Microcapsule consists of two parts, viz. the core and the wall material. The typical range of capsule content is 70 to 99% nucleus material by weight. This corresponds to a capsule wall thickness of about 0.1-200mm. Different shapes of micro capsules is shown in Figure.1

The content of capsules can be made available by mechanical rupture of the capsule wall, by causing its disintegration by electrical or mechanical means or by leaching action carried out in an appropriate liquid environment. Microcapsules range in diameter from 1 to 1000 mm; capsules greater than 1000 mm can be called microcapsules and those smaller than 1 mm are called nanocapsules.

## CHARACTERISTICS

The following are the characteristics of a microcapsule:

- Size and size distribution

Low size increases the mechanical strength as also ease of application

- Loading fraction

This is the weight ratio of core to wall of the microcapsule, the higher is this ratio the better is the production efficiency but poorer would be the stability.

- Release properties

Rate of release from microcapsules depends largely on the structure of the polymer wall, which in turn is influenced by the conditions employed in the preparation. Wall characteristics like crystallinity, cross-link density and porosity play a big role in determining the release rate. As the crystallinity and cross-link density of the wall increases, the release rate reduces substantially.

- Thermal stability

The microcapsule during its formation and application should be stable at higher temperatures.

APPLICATION OF MICROCAPSULES IN TEXTILES

The move by move developed consumer demands for textiles with new characteristics and added value into medical and technical fields has encouraged the industry to use microencapsulation processes as a means of imparting finishes and properties to fabrics which were not possible or cost-effective using other technology. Textile manufacturers are demonstrating increasing interest in the application of durable fragrances to textile as well as skin softeners; other potential application includes insect repellents, dyes, antimicrobials, phase change materials.

##### MICRO-ENCAPSULATION IN FINISHING

Micro-encapsulation of Flame Retardants

Microencapsules of di-ammonium hydrogen phosphate with polyurethane shell has been evaluated as fire retardant agent in a commercial polyurethane coating for textiles. This is achieved by melt spinning. New approaches are developed for flame retarding textiles. Micro-encapsulation of phosphates as intumescent additives, PU/clay hybrid as FR coating, PA-6/clay nano composite as FR yarn and blends of wool with high performance Fibres as heat and fire resistant barriers are investigated.

Micro-encapsulation in Medical Application

Micro-encapsulation has also found use in aromatherapy. Aromatherapy is the practice of applying and inhaling essential oils from plants as a physical and emotional boost to the body. An aromatherapy product manufactured by Kanebo is marketed under the trade name Esprit de Fleurs. Agatex has developed a technology to microencapsulate functional oils like the vitamins and Aloe Vera plant extract and use in textile finishing. It gives energetic balance to human body and also makes the fabric soft and comfortable. Number of companies has developed a technology of microencapsulating liposomes on the textile substrate which would yield controlled and targeted release of anti-cancer and anti-fungal drugs.

Micro-encapsulation of Anti-microbial agents

Anti-microbial agents are incorporated with the textile material to prevent the transmission of pathogenic microorganisms. In addition to this, antimicrobial finishes should be capable of counter attacking the development of odour from the bacterial decomposition of perspiration in clothing. Yeast cells containing biocide or insecticide have been applied to cotton, cotton wool and wool fabric. Fabrics with biocide filled yeast have been successfully tested as per AATCC Test method 100, a microbial challenge test. Mothproof agents have also been encapsulated in yeast and applied to wool fabric is also shown in figure.

Micro-encapsulation of fragrance

Our sense of smell is the strongest of our 5 senses; it is the one sense which does not rest even when we sleep. When our nose detects a change in the atmosphere around us it draws on our brains a vast memory bank to identify that change. Once identified we may be excited, soothed, relaxed, comforted, refreshed, revitalised or even alarmed. Utilising the sense of smell by building a fragrance into a textile or garment can stimulate a powerful and emotive sense. Fragrances can range from fine fragrances, florals, fruits, and malodour counteractants until aromatherapy.

Preparation of recipe

The lavender fragrance agents with binder ST were formed by mixture solution containing alcohol and distilled water with ratio (1:3). The solution was emulsified with a high-speed mixer at a speed of about 10,000 rpm for 5 minutes. The emulsified system was transferred into a flask. The alcoholic fragrance solution was added into the emulsified solutions over 30 minutes, and stirred at a temperature of 40°C for 2 hours.

Fragrance finishing was given to the fabric by exhaustion method with 5-7% binder ST which is used as cross-linking agent. The fabrics were kept immersed in the solution containing lavender fragrance, (ML ratio – 1: 10) for 20-30 minutes at 40ºC in water bath. After finishing, the fabrics were removed, squeezed and dried at 100ºC in the oven for 5 minutes and then cured at 120 ºC for 2 minutes

NANO TECHNOLOGY

Nanotechnology is a field of research and innovation concerned with building 'things' - generally, materials and devices - on the scale of atoms and molecules. A nanometre is one-billionth of a metre: ten times the diameter of a hydrogen atom. The diameter of a human hair is, on average, 80,000 nanometres.

What are nano textiles?

Nano fabrics are textiles engineered with small particles that give ordinary materials advantageous properties such as super hydro phobicity (extreme water resistance, odor and moisture elimination,increased elasticity and strength, and bacterial resistance. Depending on the desired property, a nanofabric is either constructed from nanoscopic fibers called nanofibers, or is formed by applying a solution containing nanoparticles to a regular fabric

What is nano technology clothes?

Making clothing and fabric with nanoparticles or nanofibers allows the improvement of fabric properties without a significant increase in weight, thickness, or stiffness. For example, incorporating nano-whiskers into fabric used to make pants produces a lightweight water- and stain-repellent material.

Water Repellence:

Nano-Tex improves the water-repellent property of fabric by creating nano-whiskers(a type of crystal nano fibre with a dia meter of less than 100 nm, which are hydrocarbons and 1/1000 of the size of a typical cotton fiber, that are added to the fabric to create a peach fuzz effect without lowering the strength of cotton. The spaces between the whiskers on the fabric are smaller than the typical drop of water, but still larger than water molecules; water thus remains on the top of the whiskers and above the surface of the fabric. However, liquid can still pass through the fabric, if pressure is applied. The performance is permanent while maintaining breath ability.

- Water-resistant fabric: Silica nanoparticles create a water-resistant coating when inserted into the fabric or sprayed onto the fabric surface.

UV Protective Finish:

The most important functions performed by the garment are to protect the wearer from the weather. However it is also to protect the wearer from harmful rays of the sun. The rays in the wavelength region of 150 to 400 nm are known as ultraviolet radiations. The UV-blocking property of a fabric is enhanced when a dye, pigment, delustrant, or ultraviolet absorber finish is present that absorbs ultraviolet radiation and blocks its transmission through a fabric to the skin.

Metal oxides like ZnO as UV-blocker are more stable when compared to organic UV-blocking agents. Hence, nano ZnO will really enhance the UV-blocking property due to their increase surface area and intense absorption in the UV region. For antibacterial finishing, ZnO nano particles scores over nano-silver in cost-effectiveness, whiteness, and UV-blocking property.

Fabric treated with UV absorbers ensures that the clothes deflect the Harmful ultraviolet rays of the sun, reducing a persons UVR exposure and protecting the skin from potential damage. The extent of skin protection required by different types of human skin depends on UV radiation intensity & distribution in reference to geographical location, time of day, and season. This protection is expressed as SPF (Sun Protection Factor), higher the SPF Value better is the protection against UV radiation.

- Ultraviolet-protective fabric: When inserted into fabrics, nanoparticles of zinc oxide or titanium dioxide protect the skin from sun damage. These nanoparticles have the ability to scatter the ultraviolet light present in the sun’s rays, reducing the risk of skin diseases linked to UV exposure.

Self-cleaning Fabrics:

A self-cleaning cotton fabric known as nano-care was developed and is marketed by an American Company, Nanotex and stain-resistant jeans and khakis are available since 1990.

Nanocare fabrics are created by modifying the cylindrical structure of the cotton fibres making up the fabric. At the nano scale, cotton fibres look like tree trunks. Using nano techniques, these tree trunks are covered in a fuzz of minute whiskers which creates a cushion of air around the fiber. When water hits the fabric, it beads on the points of the whiskers, the beads compress the air in the cavities between the whiskers creating extra buoyancy. In technical terms, the fabric has been rendered super-non wett able or super-hydrophobic. The whiskers also create fewer points of contact for dirt. When water is applied to soiled fabric, the dirt adheres to the water far better than it adheres to the textile surface and is carried off with the water as it beads up and rolls off the surface of the fabric. Thus the concept of Soil-cleaning is based on the leaves of the lotus plant.

Anti-static Finishes:

Static charge usually builds up in synthetic fibers such as nylon and polyester because they absorb little water. Cellulosic fibers have higher moisture content to carry away static charges, so that no static charge will accumulate. As synthetic fibers provide poor anti-static properties, research work concerning the improvement of the anti-static properties of textiles by using nanotechnology were conducted. It was determined that nano-sized titanium dioxide, zinc oxide whiskers, nano antimony-doped tin oxide (ATO) and silane nano sol could impart anti-static properties to synthetic fibers. TiO2, ZnO and ATO provide anti-static effects because they are electrically conductive materials. Such material helps to effectively dissipate the static charge which is accumulated on the fabric. On the other hand, silane nano sol improves anti-static properties, as the silane gel particles on fiber absorb water and moisture in the air by amino and hydroxyl groups and bound water.

Nano Technology for Wrinkle Free Treatment:

Nano-Tex has launched a new nanotechnology-based wrinkle-free treatment that is said to offer an improved performance while preserving fabric strength and integrity providing an alternative to harsh traditional processes. Chemicals and processing methods reduce a fabrics tear and tensile strength. This means there are certain fabrics and garments that are Wrinkle-free textiles are popular and convenient for time-pressed consumers, but traditional not candidates for wrinkle-free technology, such as lightweight fabrics or slim fitting garments. Sometimes fabrics also need to be over-engineered or beefed up in order to withstand the fiber degradation caused by traditional wrinkle-free solutions. Either way, current technologies either do not work on all fabrics or the brand/retailer has to incur additional expense just to accommodate the destructive properties of wrinkle-free chemistry.

The nano-scale molecular structure in Nano-Texs new Fortify DP technology penetrates more deeply in the fiber to improve wrinkle-free performance. Additionally, it uses a longer and more flexible cross-linking chain which reduces fiber stress under tension, thus reducing the significant strength loss associated with traditional wrinkle-free chemistry.

- Antiwrinkle cotton fabric: For cotton fabrics, wrinkle resistance can be developed by using the nano-engineered cross-linking agents during the fabric finishing process. Besides the wrinkle resistance, such finishing is also capable of eliminating toxic gases, while preserving the preferred comfort properties of cotton.

PLASMA TECHNOLOGY

What is Plasma?
When energy is continuously supplied to a matter, the temperature of the matter increases and it passes from solid state to liquid and finally to gaseous state. If the energy supply continues, the existing atomic shell disintegrates and charged particles are created (negatively charged electrons and positively charged ions). This mixture is referred to as plasma or the "fourth state of matter".

In short: Change of the aggregate state under energy supply: solid ⇒ liquid ⇒ gaseous ⇒ plasma

Plasma,  as  a  very  reactive  material,  can  be  used  to  modify  the  surface  of  a  certain  substrate , depositing chemical materials (plasma  polymerization  or  plasma  grafting)  to  impart  some  desired  properties,  removing  substances  (plasma  cleaning  or  plasma  etching)  which  were  previously  deposited  on  the  substrate.

Plasma treatment of textile fabrics and yarns is being investigated as an alternative to wet chemical fabric treatment and pretreatment processes, e.g., shrink resistant or water repellent finishing, which tent to alter fabric mechanical properties and are environmentally hazardous. The transfer of research results into the technological field would lead to non-polluting and very promising operating conditions. In the prospect of chemical finishing using plasma, two main methods can be considered: grafting of a compound on the fiber or surface modification by means of discharges. Plasma treatment modifies the uppermost atomic layers of a material surface and leaves the bulk characteristics unaffected. This treatment of textiles may result in desirable surface modifications, including but not limited to surface etching, surface activation, cross linking, chain scission, decrystallization, and oxidation. Treatment depends on the choice of working gas and plasma density and energy. Air, oxygen, argon, fluorine, helium, carbon dioxide or their mixtures can be used as plasma medium. The process result is affected by the type of the gas used. Although the gas the same, if the fiber type is different the result will be different. Textiles can be treated between two electrodes (in fact in the plasma) or near the plasma region.

Plasma-chemical conversion of the feed gas produces chemically active particles that are able to modify textile surface molecules via chemical reactions after impinging on the surface. The radicals generated inside the plasma region must be given the opportunity to move to the reaction place at the textile fiber surface. Thereby the path of radicals between the locations of generation and reaction is limited on the one hand by the Distance between single fibers and on the other hand by the gas density, i.e. by the mean distance between gas particles. Assuming radicals react or recombine after several impacts with gas particles and at surface sites on fibers there is a relationship between penetration depth of the plasma effect inside the textile structure and process pressure as well as the textile structure itself

ADVANTAGES AND DISADVANTAGES OF PLASMA TECHNOLOGY:

Advantages of the plasma technology:

Textile processing involves many stages like bleaching, finishing etc which adds value to the product. It has many constraints as it is a wet process. It utilizes large volume of water, various chemicals. It is associated with environment hazards also. Cost of processing is also a main concern. What if a new technology changes the cost structure of textile processing by reducing energy consumption, environmental waste and using fewer chemicals? Plasma-based technology can offer these benefits to textile processing industry. Off the many advantages of this technology, few are listed as:

- Applicable to most of the textile materials for surface treatment

- Optimization of surface properties of textile materials without any alternation of the inherent properties of the textile material

- It is dry textile treatment processing without any expenses on effluent treatment.

- It is a green process without the generation of chemicals, solvents or harmful substances.

- The consumption of chemicals is very low due to the physical process.

- It is applied for different kinds of textile treatment to generate more novel products to satisfy customers needs and requirements.

- It is a simple process that could be easily automated and perfect parameter control

DISADVANTAGES OF PLASMA TECHNOLOGY

Plasma treatment, however, does have certain drawbacks. The treatment tends to produce harmful gasses such as ozone and nitrogen oxides during operation. This happens due to the formation of free radicals and nascent oxygen during the treatment, which reacts with atmospheric gases to form harmful bi Products. In some cases, contaminations from the substrate such as sulfur from the crystalline links in wool can react with atmospheric oxygen to form oxides of sulfur. It is thereby recommended that plasma treatment systems are installed in well-ventilated areas to ensure that they pose no health risks for the workers working in the surrounding environment.

WATER REPELLENCY ON COTTON BY PLASMA TREATMENT

- To get water repellent effect on the substrate we can use fluorocarbon gas, siloxanes, and CH4 gas.

- The textile the substrate which we have to be functionalized is placed in the plasma chamber and then plasma ignited on to the substrate and then these molecules react with themselves forming a polymer layer directly on the substrate.

- This process produces a substrate having very low surface tension and thus the surface behaves like a water and oil-repellent fabric.

WORKING

Hydrophobic coating layers were produced by plasma polymerization of CH4. The substrate was continuously translated under the plasma deposition region at speed of 5-10 cm min2. The usable plasma area is 1 cm wide and 16 cm long. Helium or argon was used as a carrier gas (5-10 l min21) and CH4 was used as a reactive gas (10-40sccm). The power was controlled in the range of  250-400 W. Samples were mounted on a computer-controlled moving stage that traveled about 0.3-0.5 cm below the plasma source along the orthogonal direction to the plasma source head. In typical processes, the substrate was repeatedly passed back and forth across the glow-discharge plasma region at a speed of 5-10 cm min21. Here we can either use hexamethyldisiloxane gas, Fluorine, and fluorine-containing gases  (CF4, C2F6)   ETC.

Desizing of cotton fabric:
Plasma technology can be used to remove PVA sizing material from cotton fibres. In conventional desizing process we use chemicals and hot water to remove size. But desizing with plasma technology we can use either O2/He plasma or Air/He plasma. Firstly, the treatment breaks down the chains of PVA making them smaller and more soluble. X-ray photoelectron microscopy results reveal that plasma treatment introduces oxygen and nitrogen groups on the surface of PVA which owing to greater polarity increase the solubility of PVA.

Of the two gas mixtures that were studied, the results also indicate that O2/He plasma has a greater effect on PVA surface chemical changes than Air/He plasma.

Water repellent fabric:
Cotton or hemp fabric usually absorbs water immediately. Applying a low-pressure plasma process, the fibre’s surface can be altered to make it repel water. After the treatment, drops run freely over the surface while mechanical properties, the visual appearance, and the permeability for water vapour remain unchanged. The surface modification is limited to a very thin layer. A treatment as short as 2 seconds can be sufficient to achieve this effect in a batch process. Continuous treatments with a speed of more than 20 m/min are conceivable. The stability of the modification can be seen in intermitted washing cycles of fluorocarbon treated cotton fabric. After an initial drop, the finishing remains stable for at least two hours at 95°C. The quality of the repellent effect is evaluated by putting water drops to the fabric surface. A value of 1 means that the drops run freely over the surface and do not penetrate into the material while at a value of 3 the water does not penetrate but it needs vibrations to move the drop. Obviously, this evaluation depends also on the nature of the fabric.

Flame retardant fabric:
Currently, halogen-containing flame retardants are being banned for ecological reasons. The new kinds of flame-retardant chemistry, e.g. based on organic phosphonate derivatives, are much more expensive. Therefore, their usage should be limited to the absolute minimum. It has been shown that, in the case of plasma-activated fabrics consisting of both natural fibres and polymers, the concentration of flame-retardant chemicals can be reduced considerably without influencing the flame-retardant properties of the treated web. This again leads to considerable cost savings.

AQUA FINISH :

Aqua finish or textile is a range of fabrics that not only absorbs sweat quickly and efficiently, but keeps the skin feeling dry at all times. Combining  unique fabric constructions with a proprietary finishing technology. It provides maximum moisture management whether in the gym or at home. In this process special water repellency polymers are used to force the sweat from the backside of the fabric to the surface, where crimps in the yarn absorb and pull the moisture to the outside surface at incredible speed. It protects the skin from that sticky, uncomfortable feeling and never Feel The Sweat.